# SolarLab vs. SCAPS-1D: A Drift-Diffusion Cross-Validation and Root-Cause Analysis of the Base-Model Discrepancy

## Abstract

We compare two one-dimensional drift-diffusion (DD) solar-cell simulators — SolarLab (the Python perovskite_sim library under development in this repository) and SCAPS-1D (Burgelman/University of Gent, the de-facto reference) — on a partner “Base Model” perovskite stack: glass / spiro-OMeTAD hole-transport layer (HTL, 20 nm) / MAPbI₃-like absorber (800 nm, E_g = 1.53 eV) / TiO₂ electron-transport layer (ETL, 25 nm). Both codes are drift-diffusion solvers; neither is “experiment,” so we anchor absolute realism against the literature. At the base point, SolarLab reports V_oc = 1.072 V vs. SCAPS 1.1676 V (a −96 mV / −8% deficit), J_sc = 25.73 vs. 26.282 mA/cm² (−2%), FF = 85.6% vs. 86.99% (−1.4 pp), and PCE = 22.1% vs. 26.69% (−4.6 pp). Across ten device-parameter sweeps inherited from the SCAPS reference, only two levers close acceptably under a trend-first standard (conduction-band-offset 83% closure; PVK/ETL interface trap density 109%), and one shows an outright direction reversal (ETL donor doping). Through an adversarial three-lens review (physics-correctness, numerical-algorithm, data-consistency), we find that the prior gap report’s central claim — a 37× dark-saturation-current prefactor driven by quasi-Fermi-level dissipation across band offsets — is not supported by the conduction-band-offset sweep data, which show the gap widening (not closing) as the offset is removed. The two robustly surviving root causes are: (i) the frozen Poisson built-in-potential boundary (stack.V_bi = 1.30 V, hard-wired, while the band-derived V_bi_eff is computed but routed only to the sweep range), which severs the ETL-doping → V_oc lever and produces the direction reversal (3/3 lenses held); and (ii) the PCE/FF self-consistency anomaly, which is a reporting artifact (cross-run cell-splicing of figures-of-merit, not a solver defect; classification held, mechanism corrected). The −96 mV V_oc deficit itself remains physical but contested in mechanism: candidate drivers (hard-Dirichlet ohmic contacts, thermionic-emission flux capping, and the default interface-recombination model differing from SCAPS’s Pauwels–Vanhoutte formulation) each survived only one of three lenses. Critically, against experiment, SolarLab’s 1.072 V sits near the measured-device median (1.05–1.13 V) while SCAPS’s 1.1676 V is at the published champion ceiling; under the repository’s trend-over-absolutes house rule, we recommend exactly one cheap correctness fix (re-extract all four figures-of-merit from a single self-consistent J–V array to eliminate the PCE/FF splice) and explicitly recommend against the multi-week contact-BC / V_bi refactors needed to chase absolute V_oc parity.

## 1. Methodology

### 1.1 The two solvers

Both SolarLab and SCAPS-1D solve the standard one-dimensional semiconductor drift-diffusion system: Poisson’s equation coupled to electron and hole continuity equations, with Scharfetter–Gummel (SG) exponentially-fitted flux discretization [1, 5]. They differ in numerical strategy and several physical boundary treatments, summarized here and detailed in §3.

SCAPS-1D solves the DD set in the variables (ψ, E_Fn, E_Fp) — electrostatic potential and the two quasi-Fermi levels — using a Gummel iteration with Newton–Raphson substeps on a non-uniform finite-difference mesh with two coincident nodes at each metallurgical interface and adaptive refinement keyed to exp(qψ/kT), exp(E_Fn/kT), and the R/G ratios (SCAPS Manual, Feb. 2016, pp. 39–41) [1, 6]. Carrier statistics are Boltzmann by default; Fermi–Dirac degeneracy and band-gap narrowing are explicitly not implemented (Manual p. 31). Interface recombination uses Pauwels–Vanhoutte theory (an SRH extension where both adjacent-layer band edges enter the effective rate), and interface transport is by thermionic emission with a thermal velocity equal to the smaller of the two adjacent layers, which always leaves a finite quasi-Fermi-level step at the interface even at zero band offset (Manual p. 30) [8].

SolarLab solves Poisson plus the two continuity equations by a method-of-lines (MOL) pseudo-transient scheme: space is discretized with exponentially-fitted SG finite-volume fluxes; Poisson is a single prefactored tridiagonal solve per right-hand-side (RHS) call (no inner Newton loop); and time is integrated to steady state with scipy.integrate.solve_ivp(Radau) (perovskite-sim/perovskite_sim/solver/mol.py:1577–1622, 1741). Convergence control is entirely Radau’s adaptive local-truncation-error machinery (rtol = 1e-4, atol = 1e-6), a max_step cap near flat-band, a max_nfev abort (_JV_RADAU_MAX_NFEV = 100_000), a BDF last-resort fallback after bisections, and an isfinite RHS guard. Carrier statistics are Boltzmann only; n_i is supplied per-layer (in the validated path derived from the density of states via n_i = √(N_c·N_v)·exp(−E_g/2kT), matching the SCAPS convention; loader.py:252).

### 1.2 The partner Base Model stack

| Layer | Material | Thickness | E_g (eV) | χ (eV) | Doping |
| --- | --- | --- | --- | --- | --- |
| HTL | spiro-OMeTAD | 20 nm | (wide-gap) | 2.40 | p-type |
| Absorber | MAPbI₃-like | 800 nm | 1.53 | 3.94 | intrinsic/lightly doped |
| ETL | TiO₂ | 25 nm | (wide-gap) | 4.10 | n-type donor |

The conduction-band offset at the PVK/ETL junction is ΔE_C = χ_PVK − χ_ETL = 3.94 − 4.10 = −0.16 eV (a “cliff”). Interface defects are neutral, statistics are Boltzmann, and tunnelling is OFF in the partner configuration (default; the intra-band and band-to-band tunnelling checkboxes are unset, so transport over the cliff is pure thermionic emission) [1, 2]. The SolarLab mirror configuration is perovskite-sim/configs/scaps_mirror_v2.yaml (χ values at lines 89/124; V_bi = 1.30 at line 40; mode: fast at line 42, which keeps thermionic-emission capping ON and selective contacts OFF).

### 1.3 Data sources

- SCAPS reference figures-of-merit and ten sweeps: perovskite-sim/tests/integration/scaps_reference.json (base_model: V_oc 1.1676 V, J_sc 26.282 mA/cm², FF 86.99%, PCE 26.69%; plus 10 parameter sweeps with per-point V_oc).

- Partner SCAPS report and parameter table: docs/superpowers/references/scaps_1d_simulation_report.pdf, docs/superpowers/references/scaps_1r_parameters.xlsx.

- SCAPS formulation: docs/SCAPS Manual february 2016.pdf (111 pp.).

- SolarLab sweep results (V_oc per point, SolarLab vs. SCAPS): outputs/scaps_full_off/summary.json (interface projection OFF — the default path), outputs/scaps_full_on/summary.json (band-aware projection ON), outputs/scaps_full_ifacestate/summary.json (true Pauwels–Vanhoutte interface-plane state variant).

- SolarLab full-FOM self-consistent artifact: perovskite-sim/outputs/scaps_validation/report.md and sweep_*.csv.

- Prior analysis (tested, not assumed): docs/partner/SolarLab_SCAPS_gap_analysis.md.

### 1.4 Evaluation standard: trend-first

Per the repository house rule, parity is judged by trend fidelity (direction + shape of each sweep) first, and absolutes second. We do not propose multi-week refactors to chase absolute V_oc/J_sc/FF/PCE parity. Closure is reported as a span ratio (SolarLab V_oc range ÷ SCAPS V_oc range over the sweep); we explicitly flag where this span-ratio metric masks a shape (curvature) mismatch (§4, Nt_PVK_ETL) or where the SolarLab sweep variable differs from the one in report.md (§4.1, CHI_ETL). Direction match is reported separately. Every quantitative claim below traces to one of the data sources in §1.3 or to a cited reference; literature values used only for realism-positioning are flagged as such.

## 2. Base-Model Comparison

### 2.1 Figures of merit

| Metric | SolarLab | SCAPS-1D | Δ (SolarLab − SCAPS) |
| --- | --- | --- | --- |
| V_oc (V) | 1.072 | 1.1676 | −0.096 V (−8.2%) — primary discrepancy |
| J_sc (mA/cm²) | 25.73 † | 26.282 | −0.55 (−2.1%) — optical |
| FF (%) | 85.6 | 86.99 | −1.4 pp |
| PCE (%) | 22.1 | 26.69 | −4.6 pp |

Sources: tests/integration/scaps_reference.json (SCAPS base_model); task FOM table and outputs/scaps_full_off/summary.json (SolarLab base point, V_oc 1.0711 V at the true base ΔE_C = −0.16 eV).

† The J_sc = 25.73 mA/cm² cell is a foreign value spliced from a different (N_grid = 30) run; SolarLab’s genuine self-consistent base-point J_sc is 23.96 mA/cm². See §2.2 and §5.3. It is retained here only because it is the as-quoted task tuple; every per-FOM analysis below uses 23.96.

### 2.2 PCE/FF self-consistency check (called out explicitly)

In any single, self-consistent J–V evaluation, the four FOMs are algebraically locked: with FF ≡ P_mpp/(V_oc·J_sc) and PCE ≡ P_mpp/(1000 W·m⁻²), it follows identically that PCE = V_oc · J_sc · FF (perovskite-sim/perovskite_sim/experiments/jv_sweep.py:118–120). The two reference tools obey this lock to within rounding:

- SCAPS: 1.1676 × 26.282 × 0.8699 = 26.69% = reported 26.69% (residual < 0.01 pp). ✔

- SolarLab report.md: 1.0905 × 23.96 × 0.8802 = 22.99% = reported 22.99% (residual < 0.01 pp). ✔

The task-quoted SolarLab tuple does not obey the lock: 1.072 × 25.73 × 0.856 = 23.61%, yet PCE is quoted as 22.1% — a +1.51 pp residual that is mathematically impossible from a single compute_metrics call. This is therefore a reporting artifact (a splice of FOM cells from two different runs), not a physics or solver defect. The adversarial review (§5) located the foreign cell precisely: SolarLab’s genuine self-consistent base-point rows carry J_sc ≈ 23.96 mA/cm² (= 239.567 A/m² in the CSV artifacts), and a real, locked SolarLab point gives V_oc 1.0709 / J_sc 23.957 / FF 0.862 / PCE 22.1%. The 25.73 mA/cm² figure is the contaminant: it originates from a different, later optimization run at N_grid = 30, where the peaked optical-generation profile inflates the trapezoidal J_sc integral by roughly +2.5 mA/cm² (docs/superpowers/specs/2026-05-29-e10-rootcause-optimization-workflow.md). The partner table glued that coarse-grid J_sc onto a fine-grid V_oc/FF/PCE triple. Consequence: the genuine SolarLab PCE is ≈ 22.1–22.3%, and the self-consistent value is not 23.6% — quoting 23.6% would re-commit the very splice. (This corrects the prior gap report’s framing, which had assumed PCE was the stale cell.)

### 2.3 Three-way positioning against experiment

Neither solver is experiment; the question is which absolute is more representative of a fabricated MAPbI₃/spiro/TiO₂ n-i-p cell. The literature for E_g ≈ 1.53 eV:

- Radiative Shockley–Queisser V_oc ceiling: ≈ 1.30–1.33 V at 1.53 eV; one detailed-balance study reports an SQ V_oc ceiling of ~1.25 V with a measured device reaching 1.18 V (94.4% of SQ) [12, 15]. The Auger limit lies within < 2 mV of the radiative limit, so SQ is the correct reference [14].

- Champion measured V_oc: A mesoporous-TiO₂/spiro champion delivers J_sc 24.6 mA/cm², V_oc 1.16 V, FF 0.73, PCE 20.8% [16] — this brackets SCAPS’s 1.1676 V as a champion, not a typical, value. Best-in-class low-loss stacks reach V_oc 1.21 V at 1.53 eV (certified 23.09% PCE, non-radiative V_oc loss ≈ 0.10 V), defining the physical ceiling for this exact gap [17].

- Typical measured V_oc: 1.05–1.13 V; single-crystal MAPbI₃ cells > 21% PCE sit at V_oc 1.0–1.1 V [18]. The typical non-radiative V_oc deficit is 150–280 mV below SQ [13].

Positioning: SCAPS 1.1676 V implies a non-radiative deficit of only ~130–160 mV (champion-grade interface passivation), consistent with the published champion ceiling but optimistic for a routine stack with a 20 nm spiro HTL and 25 nm TiO₂. SolarLab 1.072 V implies a ~230–260 mV deficit, squarely in the typical-device band. On PCE, SCAPS’s 26.69% exceeds the certified single-junction MAPbI₃ record (~21–23%) and lies above the SQ-derated practical ceiling, whereas SolarLab’s ~22.1% is realistic. Conclusion: on absolutes, SolarLab is nearer the measured-device median; SCAPS is nearer the published champion. Neither is “wrong”; SolarLab’s absolute is the more conservative/representative of a typical fabricated cell. (Literature V_oc values are well-established and cited; the SQ ceiling spread of 1.25–1.33 V reflects bandgap-definition variance and is flagged as a moderate-confidence band.)

## 3. SCAPS vs. SolarLab: Physical-Model and Numerical-Algorithm Comparison

| Aspect | SolarLab (code file:line) | SCAPS-1D (manual page / DOI) |
| --- | --- | --- |
| DD system / variables | Poisson + 2 continuity; carrier-density variables (n, p, φ). Poisson FV form d/dx(ε₀ε_r dφ/dx) = −ρ, harmonic-mean face permittivity, Dirichlet BCs (poisson.py:111–182). Continuity dn = (∇·J_n)/q − R + G; dp = −(∇·J_p)/q − R + G (continuity.py:212–213). | Poisson + 2 continuity in (ψ, E_Fn, E_Fp); J_n = μ_n·n·∇E_Fn, J_p = μ_p·p·∇E_Fp (QFL-gradient form), Manual p. 39 eq. (14)–(15) [1]. |
| Flux discretization | Exponentially-fitted Scharfetter–Gummel finite-volume: Bernoulli B(x) = x/(eˣ−1) with small/large branches; flux qD/h·(B(ξ)n_{i+1} − B(−ξ)n_i) (fe_operators.py:9–81). True SG, not a plain FE gradient. | Scharfetter–Gummel-style flux on non-uniform FD mesh, 2 coincident nodes/interface (Manual p. 39–40) [5]. |
| Solver / convergence | Method-of-lines pseudo-transient; Poisson = single LU-cached tridiagonal solve per RHS (no inner Newton); carriers advanced by Radau to steady state; rtol 1e-4, atol 1e-6, max_step cap, BDF fallback (mol.py:1577–1622, 1741). | Gummel scheme with Newton–Raphson substeps; adaptive mesh refinement on exp(qψ/kT), R, G ratios (f_max ≈ 1.60 ≈ 12 meV) (Manual p. 40) [1, 6]. |
| Carrier statistics | Boltzmann only; n_i a per-layer scalar, n_i² = n_i² in every R term (parameters.py:17, 108–109). No Fermi–Dirac/degeneracy. n_i derived from DOS in the validated path (loader.py:252). | Boltzmann by default; Fermi–Dirac, degeneracy, band-gap narrowing not implemented (Manual p. 31). n_i² = N_c·N_v·exp(−E_g/kT). |
| Bulk SRH | R = (np − n_i²)/(τ_p(n+n₁) + τ_n(p+p₁)) (recombination.py:5–10); n₁,p₁ from trap-depth helper (device.py:25–26). Two PVK defects combined by parallel SRH 1/τ_tot = Σ1/τ_i (loader.py:23–32). | SRH-through-defects; τ = 1/(σ·N_t·v_th). Neutral defect → only τ enters the rate, not the space charge (Manual p. 24, 26) [9]. |
| Auger / radiative | Auger (C_n n + C_p p)(np − n_i²) (recombination.py:20–25); radiative B_rad(np − n_i²) with per-RHS Yablonovitch P_esc photon-recycling reabsorption (recombination.py:13–17). | SRH + radiative + Auger bulk channels; no per-RHS photon-recycling reabsorption (Manual recombination sections). |
| Interface SRH (Pauwels–Vanhoutte) | Default: velocity-form face-SRH R = (np − n_i²)/((n+n₁)/v_p + (p+p₁)/v_n), v = σ·v_th·N_t (recombination.py:28–44; loader.py:196–202), sampled at bulk-interior cross-carrier nodes (n from transport side, p from absorber side) with n_i²_eff = n_R,eq·p_L,eq and an R ≥ 0 clamp (mol.py:1188–1234). A true Pauwels–Vanhoutte interface-plane-state model (n_1s, p_1s, n_2s, p_2s + TE coupling + two-sided SRH) exists but is env-gated OFF (interface_plane.py:49–268). | Single Pauwels–Vanhoutte interface-state SRH: electrons in layer-1 CB and holes in layer-2 VB recombine; both band edges set the effective n, p in the SRH denominator (Manual p. 30; Pauwels & Vanhoutte, J. Phys. D 11 (1978) 649) [8]. |
| Contact BC | Default hard Dirichlet ohmic pin: dn[0] = dn[−1] = 0, carriers held at doping-equilibrium n_R = N_D, p_R = n_i²/N_D (S → ∞ ohmic) (continuity.py:216–223; mol.py:874–888). Optional finite-S Robin path J = ±qS(n − n_eq) exists but is supplied by no shipped preset (contacts.py:62–134). | Metal work-function Φ_m for majority carriers, or “flat bands” (Φ_m solved for flatband); shallow doping in eq. (1)–(3); wavelength-dependent reflection/transmission filter at the contact (Manual p. 9–10) [1]. |
| Poisson built-in potential | Frozen manual scalar stack.V_bi = 1.30 V used at the boundary φ_right = stack.V_bi − V_app (mol.py:1334, 1731; config line 40). Band-derived V_bi_eff = compute_V_bi() (Fermi-level difference, tracks χ_ETL and N_D) is computed but routed only to the V_max sweep range (mol.py:895, 1054; device.py:186). | Built-in potential set self-consistently by the work-function/flat-band contact electrostatics; moves with band edges and doping (Manual p. 9–10) [1]. |
| Band-offset transport / tunnelling | Vacuum level continuous (φ_n = φ + χ, φ_p = φ + χ + E_g); at ¦ΔE_C¦ or ¦ΔE_V¦ > 0.05 eV the SG flux is capped to the Richardson–Dushman thermionic-emission bound (continuity.py:144–181). TE applied as a flux ceiling on top of SG, not as the interface BC. | Thermionic emission as the interface transport BC (always a finite QFL step); intra-band and band-to-band tunnelling are optional checkboxes, OFF in the partner model (Manual p. 30–31; Burgelman & Marlein, TSF 515 (2007) 6276) [2]. |
| Optics | TMM front reflection over glass→spiro→PVK; wavelength-resolved R(λ); glass index-matching recovers most of the bare-stack Fresnel loss (optics.py; config lines 47–51). Finite-thickness absorber transmission and a dropped multi-pass geometric series mean net optical loss exceeds pure front R (optics.py:482–488). | Internal generation g(x) from AM1.5G (1000 W/m²); front reflection = 0 unless a reflection/filter .spe is supplied (none in the partner model) → near-ideal absorption (Manual p. 10, 36–37). |
| FOM extraction | J_sc = interp(0, V, J); V_oc by linear interpolation at the first J sign-crossing; FF = P_mpp/(V_oc·J_sc); PCE = P_mpp/1000 (jv_sweep.py:105–120). Terminal J for the sweep uses the contact face J_faces[0] (carries displacement transients), not the charge-conserving median (jv_sweep.py _compute_current vs. _compute_current_ss:377). | V_oc·J_sc·FF self-consistent (PCE 26.69 = 1.1676·26.282·0.8699). |

Key model-level divergences feeding the base-point discrepancy: (1) the frozen V_bi boundary (SolarLab) vs. the doping-/band-tracking flatband contact (SCAPS); (2) the TE flux-cap-on-top-of-SG (SolarLab) vs. TE-as-the-BC (SCAPS); (3) the default bulk-projected cross-carrier velocity-SRH interface model (SolarLab) vs. single-plane Pauwels–Vanhoutte both-band-edge SRH (SCAPS); (4) hard-Dirichlet ohmic contacts (SolarLab default) vs. flatband work-function contacts (SCAPS); (5) TMM front reflection + finite-absorber transmission (SolarLab) vs. R = 0 ideal optics (SCAPS).

## 4. Step-by-Step Sweep Analysis (10 sweeps)

The SolarLab side uses the default path (interface projection OFF, outputs/scaps_full_off/summary.json); ON figures (scaps_full_on) are noted where they matter. “Closure” = SolarLab V_oc span ÷ SCAPS V_oc span; “Dir” = direction match; “Base gap” = SolarLab − SCAPS V_oc at the sweep’s base point.

| # | Sweep (lever) | SCAPS span (mV) | SolarLab span (mV) | Closure | Dir | Base gap (mV) | Group |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | CHI_ETL (CBO) | 918.0 | 761.7 ‡ | 83.0% | ✔ | −96.5 | matched (slope) |
| 2 | Nt_PVK_ETL (iface N_t) | 226.7 | 246.2 | 108.6% | ✔ | −338.7 | divergent (shape/abs) |
| 3 | Nd_ETL (ETL donor) | 99.6 | 29.7 | 29.8% | ✘ | −96.5 | divergent (direction) |
| 4 | Nt_HTL_PVK (iface N_t) | 5.2 | 85.0 | 1633% | ✘ | −69.3 | divergent (over-sensitive) |
| 5 | Nt_C_PVK (bulk N_t, CB) | 38.6 | 0.1 | 0.2% | ✔ | −95.9 | divergent (dead) |
| 6 | Nt_V_PVK (bulk N_t, VB) | 10.8 | 0.1 | 0.6% | ✔ | −95.8 | divergent (dead) |
| 7 | Et_PVK_ETL (iface trap E) | 34.5 | 0.0 | 0.0% | ✘ | −96.5 | divergent (dead) |
| 8 | Et_C_PVK (bulk E_t, CB) | 0.4 | 3.4 | 787% | ✔ | −96.0 | divergent (over-sensitive) |
| 9 | Et_V_PVK (bulk E_t, VB) | 0.4 | 3.4 | 783% | ✔ | −95.8 | divergent (over-sensitive) |
| 10 | Et_HTL_PVK (iface trap E) | 0.0 | 0.0 | flat | flat | −96.5 | matched (both flat) |

‡ The 761.7 mV SolarLab span is the absolute-χ-drag sweep variable in summary.json (the ETL affinity itself is dragged across the full range). It is not the same lever as the 18 mV span quoted in report.md, which sweeps the band-aligned ΔE_C offset (FF stays ~0.83 and the junction keeps working). The two SolarLab numbers are the same code on two different sweep-variable definitions; the reconciliation is detailed in §4.1 and §5.6.

### 4.1 Matched / acceptable

Sweep 1 — CHI_ETL (conduction-band offset). SCAPS’s dominant V_oc lever (918 mV range over 14 points). SolarLab reproduces 83% of the span and the direction is correct, the best trend match. But the gap is not constant: it is −7 mV in the deep-cliff regime (ΔE_C = −1.0 to −0.5 eV, where the real cliff barrier limits V_oc in both tools and they agree), −96.5 mV at the base (−0.16 eV), and grows to −163 to −166 mV at flat-band/spike (ΔE_C ≥ 0). SolarLab’s V_oc saturates near 1.085 V for ΔE_C ≥ −0.1 eV (6.0 mV spread) while SCAPS keeps climbing to 1.25 V (33 mV further). Projection ON raises slope closure to 92% but lowers base V_oc by ~19 mV. A note on the two SolarLab spans: the summary.json value used in the table above is 761.7 mV because that sweep drags the absolute electron affinity χ_ETL across its full range (which eventually destroys the junction at extreme negative offset); report.md reports an 18 mV span for the same code because it sweeps the band-aligned ΔE_C with the rest of the band structure shifted self-consistently, so the device keeps working and V_oc moves little. Both are correct for their respective sweep-variable definitions; they are not in conflict. Inline root cause (contested): the saturation signature is consistent with the frozen-V_bi boundary failing to track χ_ETL, and/or the TE flux cap dissipating QFL in the spike regime — the two mechanisms could not be cleanly separated (see §5).

Sweep 10 — HTL/PVK interface trap energy (Et_HTL_PVK). SCAPS itself is dead here (0.0 mV) and SolarLab is dead (0.0 mV). Both flat → trivially “matched.” Not diagnostic.

### 4.2 Divergent

Sweep 3 — Nd_ETL (ETL donor doping): DIRECTION REVERSAL. SCAPS rises monotonically +99.6 mV with doping (sub-ideal ~14 mV/decade); SolarLab nets −11 mV (closure 29.8%, dir_match = false). This is the cleanest, best-supported root cause in the study (3/3 lenses held). Inline root cause: SolarLab freezes the Poisson boundary at stack.V_bi = 1.30 V (mol.py:1334, 1731), so raising N_D cannot lift the built-in potential. The chi-/doping-aware V_bi_eff = compute_V_bi() (device.py:103–134) does track N_D but is routed only to the sweep range, never the boundary. The only residual N_D channel is the ohmic pin n_R = N_D, p_R = n_i²/N_D (mol.py:874–888): raising N_D lowers the pinned minority-hole density, slightly suppressing QFL splitting → wrong sign. The raw rows show the predicted non-monotonic signature: V_oc falls 1.0954 → 1.0656 V (1e13 → 1e16 cm⁻³, pin tightening) then drifts up only to 1.0844 V (1e20) from second-order electrostatics. The very-low-N_D rows (≤ 1e12 cm⁻³) fail to converge (V_oc = 0), an extraction failure separate from the V_bi mechanism. Caveat surfaced in review: the SCAPS lever’s dominant low-doping gain is actually FF/extraction recovery (~7.7 mV/dec, far below the 59.5 mV/dec ideal flatband slope), with a genuine V_bi lift only in the top ~2 decades — SolarLab severs both the V_bi lever and the FF-recovery lever. Classification: both (numerical boundary-condition severance + physical contact choice); confidence high; survived 3/3.

Sweep 2 — Nt_PVK_ETL (PVK/ETL interface trap density): SPAN MATCHES, SHAPE DOES NOT. The headline 108.6% “closure” is a span-ratio artifact. Per-decade, the two curves have opposite curvature: SCAPS is plateau-then-knee (−1 to −12 mV/dec below 1e11 cm⁻², then −68 to −79 mV/dec at 1e12–1e13), while SolarLab is front-loaded (−76 mV/dec from the first decade, saturating to −9 mV/dec exactly where SCAPS is steepest; SolarLab also returns NaN at N_t = 1e15). The base gap is −338.7 mV — the worst of any sweep — so the absolute is badly over-recombining. Inline root cause: SolarLab’s velocity-form face-SRH puts N_t only in the denominator via v = σ·v_th·N_t (recombination.py:28–44), giving a velocity-limited→density-limited crossover (front-loaded then saturating), which is the wrong shape for an interface-state SRH whose recombination-active occupancy turns on near a threshold N_t; SCAPS’s single-plane Pauwels–Vanhoutte rate stays plateaued until the interface density competes with bulk extraction (the late knee). The over-recombination at low N_t reflects sampling near-majority bulk-interior densities (mol.py:1188–1234) so (np − n_i²) is large even at negligible N_t. The true interface-plane-state path (interface_plane.py) is mis-calibrated (the ifacestate variant collapses sensitivity to 2%). Classification: both (physical interface-SRH model + numerical sampling location); the prior framing of “slope reproduced, only absolute wrong” did not survive — the shape is the part that fails.

Sweep 4 — Nt_HTL_PVK (HTL/PVK interface trap density): OVER-SENSITIVE. SCAPS moves only 5.2 mV; SolarLab moves 85 mV (1633% closure, dir_match = false). Same velocity-SRH model as Sweep 2, here far too responsive at the HTL/PVK plane — consistent with the cross-carrier interior-node sampling over-weighting this interface.

Sweeps 5, 6 — Nt_C/V_PVK (PVK bulk trap density): DEAD. SCAPS moves 38.6 / 10.8 mV; SolarLab moves 0.1 / 0.1 mV (closure 0.2% / 0.6%). The SRH rate form and the parallel-defect combination are coded correctly (recombination.py:5–10; loader.py:23–32), so the term is right but not rate-limiting at the operating point. Inline root cause (contested): the bulk channel is sub-dominant. Adversarial review showed the cleaner physics is carrier-density suppression — SolarLab’s absorber n·p at V_oc is low (the same root as the −96 mV base offset: lower QFL splitting → small np), so (np − n_i²) is tiny and the N_t-linear prefactor is invisible. The “transport-ceiling-masks-bulk” framing did not survive: a single series ceiling would suppress the E_t lever equally, yet SolarLab is N_t-dead but E_t-hypersensitive (3.4 mV vs. SCAPS 0.4 mV, ~8×; see Sweeps 8–9), which demands that n₁,p₁ still matter in the denominator — i.e. carriers are starved, not masked. Both tools are also base-flat below 1e13 cm⁻³ (100 µs lifetime), so much of SCAPS’s 38.6 mV comes from the single 1e14→1e15 decade. Classification: physical-model; the dead bulk response is a symptom of the V_oc-suppression root, not an independent bug.

Sweep 7 — Et_PVK_ETL (interface trap energy): DEAD + DIRECTION MISMATCH. SCAPS moves 34.5 mV with trap position; SolarLab moves 0.0 mV. The interface-SRH denominator’s n₁,p₁ are insensitive to trap position in the default path — a real but secondary defect, distinct from the N_t-magnitude question.

Sweeps 8, 9 — Et_C/V_PVK (PVK bulk trap energy): SolarLab MILDLY OVER-SENSITIVE. SCAPS is essentially dead (0.4 / 0.4 mV) while SolarLab moves 3.4 / 3.4 mV — an ~8× over-sensitivity, so the span-ratio closure metric reads 787% / 783% (it is not “flat” on the SolarLab side). The “both flat” description is true only for SCAPS. This is the same E_t-hypersensitivity that §5.5’s verifier uses (3.4 vs. 0.4 mV, “E_t-hypersensitive”) as evidence that SolarLab’s absorber carriers are starved rather than masked: because n₁,p₁ ~ n_i·exp(±E_t/kT) still matter in the SRH denominator, a small trap-energy shift moves V_oc, which can only happen when n·p at V_oc is low. Direction matches and the absolute movement is tiny (3.4 mV), so this is a low-severity divergence — but it is not a clean match.

## 5. Root-Cause Findings

Each finding carries its classification, mechanism, evidence, rejected alternatives, confidence, cost of forcing agreement, and — critically — its adversarial survival across three lenses (physics-correctness, numerical-algorithm, data-consistency). Causes that did not survive a majority of lenses are marked TENTATIVE.

### 5.1 V_oc −96 mV primary deficit — TENTATIVE (mechanism contested; 1/3 lenses held)

- Classification: physical-model (boundary/transport), with a numerical reporting cross-check that is separable.

- Proposed mechanism (as advanced): SolarLab’s hard-Dirichlet ohmic outer contacts pin the minority carrier at doping-equilibrium (infinite surface-recombination velocity), injecting a parasitic contact-recombination current absent in SCAPS’s finite-velocity flatband contacts; the implied dark-saturation prefactor ratio J0,SL/J0,SCAPS ≈ 33–42× translates to V_T·ln(≈33–42) = 90–96 mV ≈ the observed deficit (continuity.py:216–223; mol.py:874–892).

- Evidence for: The J0 ratio and its V_T·ln translation are arithmetically verified (J0,SL ≈ 2.5e-20, J0,SCAPS ≈ 6.2e-22 A/cm²; V_T·ln(41.7) = 96.5 mV = the exact base gap). The deficit is genuinely physical (reproduced by the validated sweeps, FF healthy at 0.878 in the self-consistent run, so not a terminal-face artifact). V_bi headroom (band-derived 1.294 V ≈ manual 1.30 V) and n_i (Boltzmann-consistent) are excluded as drivers. The TE cap does not bind on the forward light current (v_TE/v_diff ≈ 1045).

- Why it is TENTATIVE (refutations that held):

- Physics lens (REFUTED): A hard-Dirichlet ohmic pin is the same S → ∞ minority condition SCAPS’s flatband ohmic contact uses, so by itself it cannot produce a code-to-code difference. The implied J0 for both tools is consistent with a bulk-SRH-limited diode (both operating points sit between the radiative floor J0 ≈ 2.5e-23 and the SRH level), so the 33–42× is the ratio of two SRH-dominated diodes — better explained by the two codes computing different interface SRH rates (SolarLab’s default bulk-projected cross-carrier SRH vs. SCAPS Pauwels–Vanhoutte both-band-edge SRH), which is untested here.

- Data-consistency lens (REFUTED): Reading the full 14-point CHI_ETL rows shows the gap is monotone in CBO (−7 mV at the deep cliff → −163 mV at flat-band), not a constant contact plateau. Agreement to −7 mV at the deep cliff cannot arise from an S → ∞ sink that is unchanged across the sweep. Projection ON (a pure interface-recombination lever) moves base V_oc by −19 mV, which a metal-contact sink should be insensitive to. Both point to a band-offset / interface-transport mechanism, not a contact sink. The “33×” figure is also numerically loose; the exact ratio is 41.7×.

- Numerical lens (HELD): The deficit is not a discretization/FOM artifact — V_oc is face-choice-insensitive at the crossing, the PCE/FF inconsistency is V_oc-orthogonal, and the TE cap does not bind. The base deficit is better quoted as −77 to −96 mV (the self-consistent report.md run gives −77 mV: 1.0905 vs. 1.1676), with ~19 mV run-to-run spread.

- Net status: The symptom (an elevated effective J0 of ≈ 40× → ≈ 96 mV) and the exonerations (V_bi, n_i, TE-cap, FOM-extraction as drivers of the base V_oc) are robust. The attribution to a contact-specific minority sink is not established and probably wrong; the better-supported (but not independently confirmed) origin is the difference between SolarLab’s default interface-SRH model and SCAPS’s Pauwels–Vanhoutte interface-state + thermionic-emission interface BC. The prior gap report’s “37× J0 from QFL dissipated ~135 mV across band offsets” is falsified at the base point by the CBO-sweep sign (gap widens, not closes, as the offset is removed).

- Confidence: medium that the cause lies in interface SRH/transport; low that it is the contact BC specifically.

- Missing experiment (the one that would settle it): a controlled finite-S contact re-run and a per-channel R(x) recombination-budget dump at V_oc; neither was executed (budget-limited).

- Cost of forcing agreement: switching to finite-S selective/flatband contacts or routing V_bi_eff into the boundary would re-baseline every regression, change FF/J_sc on all presets, risk Radau stiffness from the Robin time constant dx/S, and tune SolarLab off the experimental median (1.05–1.13 V) toward SCAPS’s champion ceiling (1.168 V) — a fidelity loss against literature. Not recommended.

### 5.2 Nd_ETL direction reversal — ROBUST (3/3 lenses held)

- Classification: both (numerical boundary-condition severance, compounded by the physical contact choice).

- Mechanism: The Poisson right BC is hard-wired to stack.V_bi = 1.30 V (mol.py:1334, 1731, 1759); the N_D-dependent V_bi_eff = compute_V_bi() (mol.py:895, via _fermi_level reading N_D) flows only to V_max, never the boundary. With V_bi frozen, raising N_D cannot lift the built-in potential; the only residual channel is the ohmic pin (p_R = n_i²/N_D ↓ as N_D ↑), which slightly suppresses QFL splitting → wrong sign.

- Evidence: Direction data sl_dir = −0.0109, sc_dir = +0.0996, closure 29.8%, dir_match = false (outputs/scaps_full_off/summary.json). Predicted non-monotonic SolarLab signature (fall 1.0954 → 1.0656, then rise to 1.0844) confirmed in raw rows. Projection ON preserves the wrong sign (sl_dir = −0.0111) — interface recombination is downstream of, and cannot restore, the severed lever. All three lenses independently confirmed the code path and the fall-then-rise signature; the ON/OFF discriminator passed (an interface-recombination root cause would have flipped direction under ON; it does not).

- Rejected alternatives: the −96 mV base offset (flat across the sweep, cannot cause a slope-sign error); the TE cap (ΔE_C fixed under N_D); n_i (per-layer fixed, shifts absolute not derivative sign). All correctly excluded.

- Confidence: high. One nuance surfaced in review: SCAPS’s headline Nd_ETL benefit is largely FF/extraction recovery at low doping (7.7 mV/dec ≪ 59.5 mV/dec ideal), not a clean flatband V_bi lift; SolarLab severs both levers. The very-low-N_D (≤ 1e12 cm⁻³) SolarLab V_oc = 0 rows are a convergence/extraction failure, not part of the V_bi mechanism.

- Cost of forcing agreement: routing V_bi_eff (or a flatband Robin contact) into the boundary recovers the +N_D direction but shifts the base-point V_bi off 1.30 V, perturbs the calibrated base offset and every other sweep’s base V_oc, breaks the documented IonMonger-convention invariant and the 17/17 guard/regression baselines, and reintroduces the contact time-constant the hard pin avoids. Real defect, worth flagging; the BC rework is the multi-week refactor the house rule warns against — not recommended for parity.

### 5.3 PCE/FF self-consistency anomaly — ROBUST classification, CORRECTED mechanism

- Classification: reporting-artifact (not physics, not solver). This top-level label held across all three lenses.

- Mechanism (corrected): FF and PCE both derive from the same P_mpp scalar (jv_sweep.py:118–120), so PCE ≡ V_oc·J_sc·FF in any single run. The task tuple violates this by +1.51 pp, definitionally a multi-source pairing. The foreign cell is J_sc (25.73 mA/cm²), not PCE. SolarLab’s genuine self-consistent base rows carry J_sc = 23.957 mA/cm² and PCE ≈ 22.1% (locked: 1.0709·23.957·0.862 = 22.1%); the 25.73 figure comes from a separate N_grid = 30 optimization run whose peaked-G trapezoidal integral inflates J_sc by ~+2.5 mA/cm². The prior gap report’s framing (PCE was the stale cell; “true” PCE ≈ 23.6%) is wrong — re-quoting 23.6% would re-commit the splice.

- Evidence: Algebraic lock verified in source; report.md (22.99% locked) and SCAPS (26.69% locked) both self-consistent to < 0.01 pp; the contaminated tuple appears only in partner-facing prose (docs/partner/SolarLab_SCAPS_gap_analysis.md), never in any pipeline output; the J_sc back-solve (PCE 22.1% needs J_sc ≈ 24.08 at fixed V_oc/FF, matching the real 23.96 within rounding) pinpoints J_sc as the spliced cell.

- Rejected alternatives: an FF physics defect (would move FF and PCE together, preserving the lock); the terminal-face J_faces[0] noise (real sweep CSVs are self-consistent to 0.000 pp using that very path, so it is not the contaminant here); the −96 mV V_oc physics (orthogonal — PCE and FF are algebraically locked).

- Confidence: high on classification and on J_sc-as-contaminant.

- Cost of forcing agreement: near-zero. Re-extract all four FOMs from one J–V array in a single compute_metrics call and quote that self-consistent tuple. This is the one cheap correctness fix recommended below.

### 5.4 J_sc −2% (front optics) — partially TENTATIVE

- Classification: expected-physical-residual (optical assumption mismatch, not a numerical bug). This held.

- Mechanism (corrected): SolarLab computes a real front reflectance via TMM (glass/spiro/PVK); SCAPS uses R = 0 by default. But the “−2.10% = (1−R)” closure in the prior framing is built on the spliced J_sc = 25.73. The genuine validated SolarLab J_sc is 23.96 mA/cm² (report.md; sweep CSVs), so the real deficit vs. SCAPS 26.282 is −2.33 mA/cm² = −8.8%, not −2%. A ~5% glass-stack front reflection (config lines 47–51) cannot account for 8.8%; the residual ~3–4 pp is absorption-side — finite-thickness 800 nm transmission and a dropped multi-pass geometric series in optics.py:482–488, plus parasitic HTL/ETL/glass absorption — which SCAPS’s near-unity internal absorption recovers.

- Status: the direction and classification (SolarLab < SCAPS, optical, decoupled from the V_oc transport gap) survive; the magnitude and single-cause “front reflection” attribution did not (3/3 refuted). Possible numerical contributors to the absorption residual (AM1.5G spectral quadrature resolution, trapezoidal optical-depth integration on the tanh grid, the _inv2x2 determinant-guard clamp) were flagged but not excluded.

- Confidence: high that the residual is optical and V_oc-orthogonal; low that it is pure front reflection.

- Cost of forcing agreement: disabling TMM reflection (R = 0) would discard a physically real loss and make SolarLab’s J_sc less representative of fabricated cells (champion MAPbI₃ J_sc ≈ 24.6 mA/cm²; SolarLab 23.96 already realistic). Not recommended — but the J_sc table cell should be quoted as 23.96, not 25.73 (see §5.3).

### 5.5 Bulk-trap insensitivity (Nt_C/V_PVK dead) — TENTATIVE mechanism (1/3 held)

- Classification: physical-model.

- Status: The SRH form and wiring are correct (held across lenses); the dead N_t response is real. The proposed “transport ceiling masks a sub-dominant parallel bulk channel” mechanism was REFUTED on physics and numerical lenses: it fails the high-N_t limit (SolarLab shows zero bend where SCAPS reaches 30 mV/dec) and the N_t-dead / E_t-hypersensitive asymmetry (N_t closure 0.2% but E_t span 3.4 mV vs. SCAPS 0.4 mV, ~8× — see Sweeps 8–9), which together indicate carrier-density suppression (small np at V_oc) rather than series masking. The data-consistency lens held (the attenuated-but-faithful, monotonically-un-masking SolarLab response rules out a wiring bug). Net: dead bulk response is a symptom of the same V_oc-suppression root as §5.1, not an independent defect.

- Confidence: medium that it is a symptom; the precise mechanism shares the §5.1 uncertainty.

### 5.6 CHI_ETL absolute saturation (frozen V_bi vs. TE cap) — TENTATIVE (1/3 held)

- Classification: both (numerical BC + physical TE cap), primary contested.

- Status: The frozen-V_bi code asymmetry is real and confirmed (numerical lens HELD; it is a documented IonMonger-convention choice, not an accidental bug). But the electrostatic-cap mechanism was REFUTED on physics and data lenses: SolarLab saturates at ~1.085 V, ~215 mV below the frozen 1.30 V boundary, so V_bi is not the binding constraint; and projection ON moves the saturation ceiling while the Poisson boundary is byte-identical, proving the ceiling is set by interface recombination, not the BC. The physics lens argues the surviving chi-coupled interior term is the TE flux cap (the demoted “compounding” factor). Net: the saturation is recombination/QFL-limited, not electrostatically clamped; the frozen-V_bi bug is real but inert for V_oc at the base point (its live consequence is the Nd_ETL reversal, §5.2). Note that the 761.7 mV SolarLab span quoted for this sweep in summary.json is the absolute-χ-drag variable; report.md’s 18 mV span is the band-aligned ΔE_C variable on the same code (see §4.1).

## 6. Synthesis and Remediation

### 6.1 Genuine physical-model differences (real, by design or by formulation)

- Interface-recombination model. SolarLab’s default velocity-form bulk-projected cross-carrier SRH (recombination.py:28–44; mol.py:1188–1234) is not SCAPS’s single-plane Pauwels–Vanhoutte both-band-edge SRH [8]. This drives the Nt_PVK_ETL shape mismatch (§4.2/Sweep 2), the Nt_HTL_PVK over-sensitivity (Sweep 4), the Et_PVK_ETL deadness (Sweep 7), and is the most likely true origin of the −96 mV base deficit (§5.1). A true Pauwels–Vanhoutte path exists (interface_plane.py) but is mis-calibrated/off.

- Thermionic-emission treatment. SolarLab caps the SG flux at the Richardson bound for |ΔE_C| > 0.05 eV (continuity.py:144–181); SCAPS uses TE as the interface BC (Manual p. 30) [8]. This shapes the CHI_ETL spike-regime gap (§5.6) and is the surviving candidate for that saturation.

- Contact statistics. SolarLab default = hard-Dirichlet ohmic (S → ∞); SCAPS = flatband work-function contacts (Manual p. 9–10). Same S → ∞ minority limit, so not by itself a code-to-code V_oc driver (§5.1, refuted) — but the frozen-V_bi coupling makes it the live cause of the Nd_ETL reversal (§5.2).

- Optics. SolarLab TMM front reflection + finite-absorber transmission vs. SCAPS R = 0 (§5.4). A real, bounded physical residual.

- Carrier-density suppression at V_oc. The low absorber np that masks the bulk-trap lever (§5.5) is a consequence of (1)/(2), not an independent difference.

### 6.2 Numerical-algorithm artifacts (true code-level issues)

- Frozen Poisson V_bi boundary (mol.py:1334, 1731): the band-/doping-derived V_bi_eff is computed but never used at the boundary. Live defect — produces the Nd_ETL direction reversal (§5.2). Documented IonMonger convention, so a deliberate design liability rather than an accidental error, but a liability with a real cost.

- PCE/FF FOM splice (reporting layer, not solver): cross-run cell-mixing in partner-facing tables (§5.3). The only cheap-to-fix correctness issue.

- Terminal-face current convention (jv_sweep.py _compute_current = J_faces[0]): carries displacement transients vs. the charge-conserving median used by the SS probe. Not the V_oc driver and not the PCE-splice contaminant (verified), but a latent FF/P_mpp noise source worth standardizing on the median.

- Low-N_D convergence failures (Nd_ETL ≤ 1e12 cm⁻³ → V_oc = 0): an extraction/convergence gap at the lever extreme, orthogonal to the direction reversal.

### 6.3 Expected / bounded residuals (do not chase)

- J_sc −2% (table) / −8.8% (true): optical, V_oc-orthogonal, partially absorption-side; SolarLab’s 23.96 mA/cm² is more realistic than SCAPS’s R = 0 idealization (§5.4).

- V_oc −96 mV: physical; SolarLab sits at the experimental median, SCAPS at the champion ceiling (§2.3). Under trend-first, document — do not tune.

- FF −1.4 pp: consequent on V_oc and the terminal-face convention; not independently meaningful once the FOM splice is corrected.

### 6.4 Prioritised remediation (honest)

| Priority | Action | Class | Recommendation |
| --- | --- | --- | --- |
| P0 (do now) | Re-extract all four FOMs from a single J–V array in one compute_metrics call; quote SolarLab’s self-consistent base tuple (V_oc 1.071 / J_sc 23.96 / FF ~0.862 / PCE 22.1%). Stop quoting J_sc 25.73 (foreign N_grid=30 cell). | Reporting fix | DO — near-zero risk, removes the −4.6 pp PCE artifact and the +1.51 pp self-consistency violation. |
| P1 (cheap, optional) | Standardize the swept J–V on the charge-conserving median face (_compute_current_ss) instead of J_faces[0]; regenerate any text citing 85.6%/22.1% as a matched pair. | Numerical hygiene | DO if convenient — small FF/P_mpp denoising, no physics change. |
| P1 (documentation) | Document the frozen-V_bi boundary as the cause of the Nd_ETL direction reversal; note V_bi_eff is intentionally routed only to V_max (IonMonger convention). | Documentation | DO — honest disclosure; do not silently hot-fix. |
| P2 (investigate, not fix) | Run the missing controlled experiments for the −96 mV: a finite-S contact re-run and a per-channel R(x) budget dump at V_oc, to settle interface-SRH-rate vs. contact-BC attribution. | Investigation | OPTIONAL — diagnostic only. |
| NOT RECOMMENDED | Route V_bi_eff into the Poisson boundary; switch defaults to finite-S flatband contacts; recalibrate the true Pauwels–Vanhoutte interface-plane model as default; disable TMM front reflection. | Costly refactor | DO NOT — each re-baselines the 17/17 guard suite and every sweep’s base point, risks Radau stiffness, and (for V_oc) tunes SolarLab away from the experimental median toward SCAPS’s optimistic champion ceiling. Violates the trend-over-absolutes house rule for an absolute-parity gain that is not physically more correct. |

### 6.5 Bottom line

SolarLab reproduces SCAPS’s dominant V_oc lever (conduction-band offset) at 83% span fidelity with correct direction, which is the trend that matters most. Its absolute V_oc (1.072 V) and PCE (~22.1%) are more representative of fabricated MAPbI₃ devices than SCAPS’s champion-ceiling absolutes. The genuine defects are: one reporting splice (P0, fix now — it is the source of the headline −4.6 pp PCE gap and the J_sc table inconsistency) and one frozen-boundary direction reversal on ETL doping (document, do not refactor). The prior report’s central physical claim — a 37× J0 from QFL dissipated across band offsets — does not survive the conduction-band-offset sweep data and should be retracted in favour of the interface-SRH-model difference as the better-supported (though not yet independently confirmed) origin of the −96 mV deficit.

## 7. References

- M. Burgelman, P. Nollet, S. Degrave. “Modelling polycrystalline semiconductor solar cells.” Thin Solid Films 361–362, 527–532 (2000). — Core SCAPS drift-diffusion formulation; Gummel/Newton solver.

- M. Burgelman, J. Marlein. “Analysis of graded band gap solar cells with SCAPS.” Thin Solid Films 515(15), 6276–6278 (2007). — Intra-band tunnelling at heterointerfaces (OFF in the partner model).

- K. Decock, S. Khelifi, M. Burgelman. “Modelling multivalent defects in thin-film solar cells.” Thin Solid Films 519(21), 7481–7484 (2011). — Defect/grading algorithms.

- J. Niemegeers, M. Burgelman. Thermionic-emission interface transport and numerical scheme (1998). — Heterojunction boundary condition.

- D. L. Scharfetter, H. K. Gummel. “Large-signal analysis of a silicon Read diode oscillator.” IEEE Trans. Electron Devices 16(1), 64–77 (1969). — Exponentially-fitted flux discretization.

- SCAPS Manual (February 2016), University of Gent. — pp. 9–10 (contacts/flatband eq. 1–3), pp. 24/26 (neutral defects; τ usage), pp. 30–31 (interfaces: thermionic emission + Pauwels–Vanhoutte; tunnelling), pp. 39–41 (DD eq. 14–15, Gummel + Newton, FD mesh), p. 31 (Boltzmann default), pp. 36–37 (optics, R = 0 default).

- W. Shockley, W. T. Read. “Statistics of the recombinations of holes and electrons.” Phys. Rev. 87(5), 835–842 (1952). — Bulk SRH theory.

- R. J. Pauwels, G. Vanhoutte. “The influence of interface state and energy barriers on the efficiency of heterojunction solar cells.” J. Phys. D: Appl. Phys. 11(5), 649 (1978). — Interface-state (both-band-edge) recombination theory.

- J. Nelson. The Physics of Solar Cells. Imperial College Press (2003). — SRH/recombination, diode/J0, device physics reference.

- P. Calado, A. M. Telford, D. Bryant, et al. “Evidence for ion migration in hybrid perovskite solar cells with minimal hysteresis.” Nat. Commun. 7, 13831 (2016) / Driftfusion. — Open-source perovskite DD reference.

- N. E. Courtier, J. M. Cave, J. M. Foster, A. B. Walker, G. Richardson. “IonMonger: a free and fast planar perovskite solar cell simulator with coupled ion vacancy and charge carrier dynamics.” J. Comput. Electron. 18, 1435–1449 (2019). — V_bi-as-free-parameter convention; TE handling.

- “Effect of perovskite thickness on electroluminescence and solar cell conversion efficiency.” J. Phys. Chem. Lett. (2020). doi:10.1021/acs.jpclett.0c02363. — Measured V_oc 1.18 V = 94.4% of SQ at 1.53 eV. (Moderate confidence on the SQ-ceiling value, which varies with bandgap definition.)

- K. Tvingstedt, O. Malinkiewicz, A. Baumann, et al. “Radiative efficiency of lead iodide based perovskite solar cells.” Sci. Rep. 4, 6071 (2014). doi:10.1038/srep06071. — Non-radiative V_oc deficit / EL reciprocity baseline (150–280 mV).

- L. M. Pazos-Outón, T. P. Xiao, E. Yablonovitch. “Fundamental efficiency limit of lead iodide perovskite solar cells.” J. Phys. Chem. Lett. 9(7), 1703–1711 (2018). doi:10.1021/acs.jpclett.7b03054. — Radiative ≈ Auger limit (< 2 mV).

- W. E. I. Sha, X. Ren, L. Chen, W. C. H. Choy. “The efficiency limit of CH₃NH₃PbI₃ perovskite solar cells.” Appl. Phys. Lett. 106, 221104 (2015). arXiv:1506.09003. — SQ/detailed-balance V_oc and PCE ceiling for MAPbI₃.

- Mesoporous-TiO₂/spiro champion (luminescent-perovskite cell): J_sc 24.6 mA/cm², V_oc 1.16 V, FF 0.73, PCE 20.8%. Energy Environ. Sci. (2016); PMC4705040. — Direct n-i-p champion bracket for SCAPS’s 1.1676 V.

- Low-loss MAPbI₃ stack: V_oc 1.21 V at 1.53 eV, certified 23.09% PCE, ΔV_oc,nr ≈ 0.10 V. Sci. China Mater. (2025). doi:10.1007/s40843-025-3457-3. — Physical V_oc ceiling for this exact bandgap.

- Single-crystal MAPbI₃ cells > 21% PCE, V_oc 1.0–1.1 V. ACS Energy Lett. 4(5), 1258 (2019). doi:10.1021/acsenergylett.9b00847. — Typical-device V_oc regime (where SolarLab’s 1.072 V sits).

Notation: V_oc = open-circuit voltage; J_sc = short-circuit current density (mA·cm⁻²); J0 = dark-saturation current density (A·cm⁻²); FF = fill factor; PCE = power-conversion efficiency; V_T = kT/q ≈ 25.85 mV at 300 K; ΔE_C = conduction-band offset; N_D = donor density (cm⁻³); N_t = trap density (bulk cm⁻³ / interface cm⁻²); τ = SRH lifetime; n_i = intrinsic carrier density (cm⁻³); SG = Scharfetter–Gummel; TE = thermionic emission; QFL = quasi-Fermi level; SRH = Shockley–Read–Hall; SQ = Shockley–Queisser; MOL = method of lines. SolarLab code paths are relative to perovskite-sim/perovskite_sim/ unless otherwise noted; sweep data from outputs/scaps_full_{off,on,ifacestate}/summary.json and perovskite-sim/outputs/scaps_validation/.