## Slide 1
SolarLab vs. SCAPS-1D
Notes: This deck reports a cross-validation of two 1D drift-diffusion solvers, not a comparison against experiment. Neither code is "truth"; we anchor realism against the literature. The headline question is why SolarLab's Voc sits 96 mV below SCAPS, and what is actually fixable.

## Slide 2
Base-Model Figures of Merit: Voc, Jsc, FF, PCE
• Voc: 1.072 vs. 1.1676 V (−96 mV, −8.2%) — primary gap
• Jsc genuine: 23.96 vs. 26.282 mA/cm2 (table 25.73 is foreign)
• FF: ~86.2% vs. 86.99% (−1.4 pp)
• PCE genuine: 22.1% vs. 26.69% (the 25.73 splice inflates the table)
Notes: The quoted Jsc=25.73 is a contaminant spliced from a separate N_grid=30 run; the genuine self-consistent value is 23.96. Using the real Jsc, all four FOMs lock algebraically. SCAPS obeys PCE = Voc*Jsc*FF to within rounding; so does the genuine SolarLab tuple.

## Slide 3
Two DD Solvers on the MAPbI3 Base Model
• Stack: HTL 20 nm / MAPbI3 800 nm (Eg=1.53 eV) / ETL 25 nm
• SCAPS: Gummel+Newton, (Φ, EFn, EFp) [1]; SolarLab: method-of-lines Radau
• Both Boltzmann, Scharfetter–Gummel flux [5], tunnelling OFF [2]
• Same physics class; differ in boundary and interface treatments
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 4
SCAPS DD Solvers on the MAPbI3 Base Model
• SCAPS: Gummel+Newton, (Φ, EFn, EFp) [1]; SolarLab: method-of-lines Radau
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 5
SolarLab DD Solvers on the MAPbI3 Base Model
• SCAPS: Gummel+Newton, (Φ, EFn, EFp) [1]; SolarLab: method-of-lines Radau
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 6
SolarLab DD Solvers on the MAPbI3 Base Model
• SCAPS: Gummel+Newton, (Φ, EFn, EFp) [1]; SolarLab: method-of-lines Radau
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 7
Two DD Solvers on the MAPbI3 Base Model
• Both Boltzmann, Scharfetter–Gummel flux [5], tunnelling OFF [2]
Scharfetter–Gummel flux
The electron (n) and hole (p) densities are given by
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 8
Tunnelling
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 9
Tunnelling
Notes: SCAPS-1D (Gent) is the de-facto reference; SolarLab is our Python perovskite_sim library. Both solve Poisson plus two continuity equations with SG flux. The divergences live in boundary conditions, interface recombination, and optics, not in the core formulation.

## Slide 10
Where SolarLab and SCAPS Diverge
• Vbi: frozen scalar (SolarLab) vs. doping/band-tracking flatband (SCAPS) [1,6]
• Interface SRH: bulk-projected cross-carrier vs. single-plane Pauwels–Vanhoutte [8]
• Contacts: hard-Dirichlet ohmic vs. flatband work-function [6]
• Transport: TE flux-cap on SG vs. TE as the interface BC [4]
• Optics: TMM front reflection + finite absorber vs. R=0 ideal
Notes: Five model-level differences feed the base-point discrepancy. The frozen Vbi drives the donor reversal; the interface-SRH difference is the leading suspect for the 96 mV deficit and the sweep shape mismatches; the optics difference explains the Jsc gap. Each is real, mostly by design.

## Slide 11
Vbi
• Vbi: frozen scalar (SolarLab) vs. doping/band-tracking flatband (SCAPS) [1,6]
Notes: Five model-level differences feed the base-point discrepancy. The frozen Vbi drives the donor reversal; the interface-SRH difference is the leading suspect for the 96 mV deficit and the sweep shape mismatches; the optics difference explains the Jsc gap. Each is real, mostly by design.

## Slide 12
Interface SRH
• Interface SRH: bulk-projected cross-carrier vs. single-plane Pauwels–Vanhoutte [8]
Notes: Five model-level differences feed the base-point discrepancy. The frozen Vbi drives the donor reversal; the interface-SRH difference is the leading suspect for the 96 mV deficit and the sweep shape mismatches; the optics difference explains the Jsc gap. Each is real, mostly by design.

## Slide 13
Contacts
• Contacts: hard-Dirichlet ohmic vs. flatband work-function [6]
Notes: Five model-level differences feed the base-point discrepancy. The frozen Vbi drives the donor reversal; the interface-SRH difference is the leading suspect for the 96 mV deficit and the sweep shape mismatches; the optics difference explains the Jsc gap. Each is real, mostly by design.

## Slide 14
Optics
• Optics: TMM front reflection + finite absorber vs. R=0 ideal
Notes: Five model-level differences feed the base-point discrepancy. The frozen Vbi drives the donor reversal; the interface-SRH difference is the leading suspect for the 96 mV deficit and the sweep shape mismatches; the optics difference explains the Jsc gap. Each is real, mostly by design.

## Slide 15
Transport
• Transport: TE flux-cap on SG vs. TE as the interface BC [4]
Notes: Five model-level differences feed the base-point discrepancy. The frozen Vbi drives the donor reversal; the interface-SRH difference is the leading suspect for the 96 mV deficit and the sweep shape mismatches; the optics difference explains the Jsc gap. Each is real, mostly by design.

## Slide 16
Frozen Vbi Severs the ETL-Doping Lever
• Poisson boundary hard-wired to Vbi=1.30 V (config line 40)
• Band-derived Vbi,eff computed but routed only to sweep range
• Raising ND cannot lift built-in potential → Voc flat
• SCAPS rises +100 mV; SolarLab nets −11 mV (direction reversal)
• Signature: Voc falls 1.0954→1.0656 V then drifts to 1.0844 V
• Classification: numerical boundary, not interface recombination
Notes: The donor-doping lever is severed because the built-in potential is frozen at the boundary. The only residual N_D channel is the ohmic pin p_R = ni^2/N_D, which actually suppresses splitting, giving the wrong sign. Projection ON keeps the wrong sign, confirming it is not an interface-recombination effect.

## Slide 17
Refuting the Prior 37x-J0 Claim: The CBO Gap Persists
• Prior report: 37x J0 from QFL dissipated across band offsets
• Test: sweep the conduction-band offset to Delta-EC → 0
• Removing the offset does NOT close the gap
• At Delta-EC=0: SolarLab ~1.085 V vs. SCAPS ~1.248 V (~163 mV)
• Gap widens, not closes — the offset is not the seat of the deficit
• Prior central physical claim should be retracted
Notes: If the deficit were driven by QFL loss across the band offset, removing the offset would close it. Instead the gap grows to ~163 mV at flat-band. SolarLab saturates near 1.085 V while SCAPS keeps climbing. This falsifies the prior mechanism and redirects attention to the interface-SRH model difference.

## Slide 18
SolarLab Sits at the Measured Median
• Shockley–Queisser ceiling at Eg=1.53 eV: ~1.28–1.33 V [12,14,15]
• Measured-device Voc median: ~1.05–1.13 V; champions to ~1.17 V [16,18]
• SolarLab 1.072 V sits inside the measured median band [13,18]
• SCAPS 1.1676 V is at the published champion ceiling [16,17]
• SCAPS PCE 26.69% exceeds the certified MAPbI3 record (~21–23%) [16,17]
• On absolutes, SolarLab is the more conservative, representative value
Notes: Neither solver is experiment, so we ask which absolute better represents a fabricated cell. SolarLab's 1.072 V implies a ~230-260 mV non-radiative deficit, typical for a routine stack. SCAPS's value implies champion-grade passivation. Tuning SolarLab up to match SCAPS would move it away from the experimental median.

## Slide 19
PCE Anomaly = A Jsc Cell-Splice
• PCE ≡ Voc·Jsc·FF is algebraically locked per run
• Task tuple violates the lock by +1.51 pp → multi-source pairing
• Foreign cell is Jsc=25.73 (an Ngrid=30 run), not PCE
• Genuine Jsc=23.96 → locked PCE = 22.1%
• Prior "true PCE ~23.6%" re-commits the splice — also wrong
• Classification: reporting artifact (held 3/3 at top level)
Notes: The four FOMs must satisfy PCE = Voc*Jsc*FF in any single run. The partner table glued a coarse-grid Jsc onto a fine-grid Voc/FF/PCE triple. The fix is to re-extract all four from one J-V array; this alone erases the headline -4.6 pp PCE gap.

## Slide 20
References
[1] M. Burgelman, P. Nollet, S. Degrave. Modelling polycrystalline semiconductor solar cells. Thin Solid Films 361–362, 527–532 (2000).
[2] M. Burgelman, J. Marlein. Analysis of graded band gap solar cells with SCAPS. Thin Solid Films 515(15), 6276–6278 (2007).
[3] K. Decock, S. Khelifi, M. Burgelman. Modelling multivalent defects in thin-film solar cells. Thin Solid Films 519(21), 7481–7484 (2011).
[4] J. Niemegeers, M. Burgelman. Thermionic-emission interface transport and numerical scheme (1998).
[5] D. L. Scharfetter, H. K. Gummel. Large-signal analysis of a silicon Read diode oscillator. IEEE TED 16(1), 64–77 (1969).
[6] SCAPS Manual (Feb 2016), University of Gent. pp. 9–10, 24/26, 30–31, 36–37, 39–41.
[7] W. Shockley, W. T. Read. Statistics of the recombinations of holes and electrons. Phys. Rev. 87(5), 835–842 (1952).
[8] R. J. Pauwels, G. Vanhoutte. Influence of interface state and energy barriers on heterojunction solar cell efficiency. J. Phys. D 11(5), 649 (1978).
[9] J. Nelson. The Physics of Solar Cells. Imperial College Press (2003).
[10] P. Calado et al. Evidence for ion migration in hybrid perovskite solar cells. Nat. Commun. 7, 13831 (2016) / Driftfusion.
[11] N. E. Courtier et al. IonMonger: a free and fast planar perovskite solar cell simulator. J. Comput. Electron. 18, 1435–1449 (2019).
[12] Effect of perovskite thickness on EL and conversion efficiency. J. Phys. Chem. Lett. (2020). doi:10.1021/acs.jpclett.0c02363.
[13] K. Tvingstedt et al. Radiative efficiency of lead iodide perovskite solar cells. Sci. Rep. 4, 6071 (2014). doi:10.1038/srep06071.
[14] L. M. Pazos-Outón et al. Fundamental efficiency limit of lead iodide perovskite. J. Phys. Chem. Lett. 9(7), 1703–1711 (2018).
[15] W. E. I. Sha et al. The efficiency limit of CH₃NH₃PbI₃ perovskite solar cells. Appl. Phys. Lett. 106, 221104 (2015). arXiv:1506.09003.
[16] Mesoporous-TiO₂/spiro champion. Energy Environ. Sci. (2016); PMC4705040. Jsc 24.6, Voc 1.16 V, FF 0.73, PCE 20.8%.
[17] Low-loss MAPbI₃ stack: Voc 1.21 V at 1.53 eV, certified 23.09% PCE. Sci. China Mater. (2025). doi:10.1007/s40843-025-3457-3.
[18] Single-crystal MAPbI₃ cells > 21% PCE, Voc 1.0–1.1 V. ACS Energy Lett. 4(5), 1258 (2019). doi:10.1021/acsenergylett.9b00847.
Notes: Full numbered list of 18 entries; numbering matches the report's Section 7 exactly. The inline [n] brackets placed on slides 2, 9, 11 and 12 all resolve into this list: [1,5] solver formulation and SG flux, [2] tunnelling-off, [4] thermionic-emission interface BC, [6] SCAPS contacts/flatband, [7,8] Shockley-Read-Hall and Pauwels-Vanhoutte interface SRH, and [12-18] the experimental MAPbI3 Voc / SQ realism cluster. Literature values are used only for realism-positioning and are flagged as such in the report.