SolarLab Paper-Reproduction Validation Figure

Key point: the comparison asks whether SolarLab can reproduce the published photovoltaic benchmarks after using literature-aligned model conventions. The baseline model is the unadjusted SolarLab implementation; the literature-aligned model uses the legacy physics convention and Vbi choices needed to compare directly with the published studies.

Terminology Used in the Figure

Published benchmark: The target number or range reported in the original paper, such as Voc, Jsc, or FF.

SolarLab baseline model: The default SolarLab configuration before applying paper-specific conventions. It is useful for diagnosing why the model differs from the literature.

Literature-aligned model: The SolarLab configuration after adopting the relevant literature conventions, such as the legacy electrostatic convention, recombination setting, and built-in voltage Vbi used for the published comparison.

Panel-By-Panel Reading Guide

A: IonMonger J-V compares the SolarLab baseline model with the Courtier-aligned model. The dashed vertical line is the published Voc benchmark. The literature-aligned curve moves close to the published Voc.

B: Driftfusion J-V compares the SolarLab baseline model with the Calado-aligned model. The gray band is the published Voc range. The literature-aligned curve moves into the benchmark interval.

C: The table summarizes the numerical comparison: published benchmark, literature-aligned model value, and delta. Range deltas are computed relative to the midpoint.

D: The device configuration panel shows that both tests use the same p-i-n layer order: spiro HTL, MAPbI3 absorber, and TiO2 ETL. The main changes are physics conventions and Vbi, not the stack sequence.

E: The optics check compares Beer-Lambert and TMM optics at fixed Vbi. This separates optical-generation effects from voltage-calibration effects.

F: The Suns-Voc check confirms that the literature-aligned Driftfusion model still gives a physical logarithmic response to illumination. The slope is written as dVoc/d ln(Phi/Φ1sun), which is more formal than saying per ln-unit.

Explanation of nid in Panel F

Meaning: nid is the diode ideality factor. It is a compact indicator of how close the simulated solar cell is to ideal diode behavior.

How it is estimated: Panel F fits the slope of Voc versus ln(Phi/Φ1sun). At room temperature, kT/q is about 25.85 mV, so nid is estimated as slope divided by kT/q.

Value in this figure: The fitted slope is about 62.3 mV, giving nid ≈ 62.3/25.85 ≈ 2.4.

Physical interpretation:

nid close to 1 usually indicates more ideal diode behavior.

nid near 2 suggests trap-assisted recombination is important.

nid above 2 indicates stronger non-ideal effects, such as field-dependent recombination, interfacial recombination, ionic effects, or transport limitations.

Main Comparison Takeaway

IonMonger: the baseline Voc is about +126 mV away from the published benchmark, while the literature-aligned model is only about +5 mV away.

Changing the Beer-Lambert IonMonger Vbi from 1.10 V to 0.86 V shifts Voc by about -238 mV, showing that Vbi convention strongly controls the voltage mismatch.

Driftfusion: the baseline Voc is about -386 mV below the Calado midpoint, while the literature-aligned model is about -21 mV from the midpoint.

Jsc stays close to the Beer-Lambert paper scale in both comparisons, so the dominant discrepancy is the Voc convention rather than optical current generation.