## Slide 1
High-throughput DFT and small-sample ML for chalcogenide PV absorber discovery, with device-scale validation
Xuanyan Chen et al.
HKUST(GZ) — 3rd JMI conference 2026

## Slide 2
01
PROBLEM

## Slide 3
01 · PROBLEM
2 / 32
Efficiency–stability design space for thin-film photovoltaics
Two established regimes, one unoccupied region
• Si: indirect band gap, ~22 % single-junction PCE ceiling, T80 > 104 h
• CIGS: direct-gap chalcogenide, 23.4 % record, constrained by In and Ga reserves
• Perovskite: PCE > 26 %, T80 frequently < 500 h under 1-sun, 85 °C
• Detailed-balance limit at Eg ≈ 1.34 eV reaches 33.7 % [Shockley & Queisser 1961]
• Target region: PCE > 25 % combined with T80 > 105 h is currently unoccupied
• These constraints motivate a third absorber class with a direct or near-direct gap
SOLARLAB

## Slide 4
01 · PROBLEM
3 / 32
CIGS — Cu(In,Ga)Se2 chalcopyrite absorber
Tetragonal I-4̄2d · cation-ordered diamond-like sublattice · tunable direct gap
• Stoichiometry Cu(In,Ga)Se2; In and Ga share a single cation site at composition x = Ga / (In + Ga)
• Lattice parameters a ≈ 5.78 Å · c ≈ 11.62 Å with c / a ≈ 2 (chalcopyrite = doubled zincblende)
• Direct band gap tunable approximately linearly from 1.04 eV (CuInSe2) to 1.68 eV (CuGaSe2)
• Polycrystalline thin-film absorber 1–3 µm on a Mo back contact; CdS / ZnO buffer + window stack
• Champion lab cell PCE 23.4 % (Solar Frontier 2019); module reliability T80 > 25 yr in field
• In-free sister chalcogenide kesterite Cu2ZnSn(S,Se)4 explored at HKUST(GZ) [Yan et al. Nat. Energy 2018 · ACS Energy Lett. 2017]
SOLARLAB

## Slide 5
01 · PROBLEM
4 / 32
Perovskite — ABX3 structural family
Pm-3̄m cubic parent · corner-sharing BX6 octahedral framework
• General formula ABX3: A = Cs+ / MA+ (CH3NH3+) / FA+ · B = Pb2+ / Sn2+ · X = I / Br / Cl
• BX6 octahedra share corners; A cation occupies the 12-coordinated cuboctahedral void
• Stability set by Goldschmidt tolerance factor t = (rA + rX) / (√2 (rB + rX)); cubic perovskite for 0.9 ≤ t ≤ 1.0
• Direct band gap, strong absorption (α ≈ 105 cm−1 near band edge), long carrier diffusion lengths
• Champion single-junction PCE 26.7 % (UNIST 2024); inverted PSC 22.3 % via ligand anchoring [Hou et al. Nat. Energy 2020]
• Tandem records: monolithic perovskite / Si tandem and 24.2 % all-perovskite tandem [Hou et al. Science 2020 · Nat. Energy 2020]
SOLARLAB

## Slide 6
01 · PROBLEM
5 / 32
Limitations of the established absorbers
Record-cell PCE timeline and accelerated-aging stability gap
• Si record 27.6 % (UNSW 2024) — five decades of incremental improvement
• Perovskite record 26.7 % (UNIST 2024) — single-junction parity with Si in under a decade
• Stability gap remains > 100× under operating stress (ion migration, A-site loss, photo-induced degradation)
• Encapsulation mitigates ingress but does not address intrinsic absorber-side instability [Boyd et al. 2019]
• Module-scale commercial deployment requires both record-class efficiency and outdoor lifetime
• Motivates the discovery of new absorber chemistries that satisfy both criteria simultaneously
SOLARLAB

## Slide 7
01 · PROBLEM
6 / 32
Talk outline
Six stages connecting the materials database to predicted device performance
• 01 PROBLEM — efficiency–stability tradeoff, CIGS and perovskite definitions (5 slides)
• 02 STRATEGY — chalcogenide structural template
• 03 ML AND FEATURES — small-sample HSE06 surrogate (8 slides)
• 04 CANDIDATES — fourteen-material shortlist
• 05 BRIDGE — 1D and 2D drift-diffusion device simulation (8 slides)
• 06 PAYOFF — predicted device J–V and outlook
SOLARLAB

## Slide 8
02
STRATEGY

## Slide 9
02 · STRATEGY
7 / 32
Chalcogenide templates as the structural prior
AB2C4 and ABC3 frameworks with heavy-p-block cations on chalcogen anions
• Anion sublattice: S, Se, Te. Selenides comprise 11 of 14 shortlisted candidates, including the top six
• Active cation: Sb, Sn, Bi (6s2 / 5s2 lone pair) producing dispersive valence-band maxima
• Spectator cation: Cs, Ca, Sr, K donate charge without contracting the valence-band dispersion
• Stoichiometry preference: AB2C4 ≫ ABC3 ≈ ABC2 in the screened subset
• Symmetry distribution: Pnma (SG 62) is dominant; followed by SG 12, 14, 72 and 15
• Constrains the > 105 candidate pool to a physically plausible, synthetically accessible subspace
SOLARLAB

## Slide 10
02 · STRATEGY
8 / 32
End-to-end pipeline
MP / OQMD → ML surrogate → DFT validation → device sim → expt
SOLARLAB

## Slide 11
03
ML + FEATURES

## Slide 12
03 · ML + FEATURES
9 / 32
Motivation for a learned surrogate
Four-stage HSE06 and DFPT workflow executed in VASP for each candidate
• Stage 1 PBE relaxation → Stage 2 SCF → Stage 3 DFPT dielectric tensor → Stage 4 HSE06 band structure
• DFPT and HSE06 dominate runtime, requiring 100–102 CPU-hours per structure on a 64-core node
• PBE relaxation scales as O(N3) in plane-wave eigensolve; HSE06 adds ~10× overhead via exact exchange [Heyd et al. 2003]
• DFPT dielectric tensor obtained from the linear-response Sternheimer equation at ~2× SCF cost [Baroni et al. 2001]
• Combined MP and OQMD pool exceeds 105 candidates, rendering full-DFT enumeration computationally infeasible
• Approach: train a learned surrogate on 473 DFT-labelled materials and use it to rank the unlabelled pool
SOLARLAB

## Slide 13
03 · ML + FEATURES
10 / 32
Hand-crafted feature set (167 D)
Composition · structure · symmetry — Magpie + matminer
• Composition (~27 D): Magpie statistics over Z, χ, atomic radius, row, group, mass [Ward et al. 2016]
• Magpie reduces a formula AaBbCc to mean / std / min / max / mode of element properties weighted by stoichiometry
• Structure (140 D): CrystalNN site-fingerprint (122) + RDF + density + packing [matminer · Ward et al. 2018]
• All featurisers tolerate NaN — routed to the appropriate side of every HistGBR split
• Cached numpy matrices on disk → re-fits run in seconds, not minutes
• Frozen MEGNet 16-D embeddings give R2 = 0.366 — below hand-features baseline [Chen et al. 2019]
SOLARLAB

## Slide 14
03 · ML + FEATURES
11 / 32
Composite photovoltaic figure of merit
Four physically motivated factors combined into a single scalar target y ∈ [0, 1]
• y = fgap(Eg) · 1 / (1 + mavg) · tanh(ε / 10) · 1 / (1 + Eb / 0.1)
• fgap(Eg): triangular Shockley–Queisser window peaked at 1.34 eV, vanishing at 0.5 and 2.5 eV
• 1 / (1 + mavg): monotonic decay rewarding low effective mass and therefore high mobility
• tanh(ε / 10): saturates above ε ≈ 10 to reflect diminishing returns from dielectric screening
• 1 / (1 + Eb / 0.1): favours Wannier–Mott regimes (Eb < 0.1 eV) and penalises Frenkel-exciton systems
• Bounded, differentiable, physically interpretable; replaces four independent regression heads with one
SOLARLAB

## Slide 15
03 · ML + FEATURES
12 / 32
Histogram-based gradient boosting regression
Stage-wise additive function approximation [Friedman 2001 · Ke et al. 2017]
• Fm(x) = Fm-1(x) + ν · hm(x), where hm fits the negative gradient of the loss at Fm-1
• Histogram binning into 256 discrete buckets reduces a split scan from O(N) to O(B), yielding ~3× speedup
• Native NaN handling: missing values learn an independent split direction at each tree node
• Hyperparameters: 600 boosting iterations · maximum depth 4 · learning rate 0.05 · minimum samples per leaf 10
• Target wrapped in log1p(y / 0.08) by TransformedTargetRegressor; inverse via 0.08 · expm1
• Logarithmic transform compresses the heavy-tailed PV-score distribution and equalises booster resolution near peak (y ≈ 0.5) and bulk (y ≈ 0.01)
SOLARLAB

## Slide 16
03 · ML + FEATURES
13 / 32
Gaussian-process and random-forest uncertainty stack
Matérn-5/2 kernel with additive white noise [Rasmussen & Williams 2006]
• k(x, x') = σf2 (1 + √5 r + (5/3) r2) exp(−√5 r) + σn2 δ(x − x')
• r = ‖x − x'‖ / ℓ; the anisotropic length-scale ℓ is optimised by L-BFGS-B on the marginal log-likelihood
• White-noise variance σn2 absorbs DFT scatter, typically 0.02 – 0.05 on the log target
• A random-forest predictor (300 trees) compensates for GP underconfidence in sparsely sampled regions
• Stack mean: μ(x) = wGP μGPR + wRF μRF · variance: σ2(x) = wGP2 σGPR2 + wRF2 σRF2
• Mixing weights are obtained via non-negative ridge regression on out-of-fold predictions, ensuring calibration
SOLARLAB

## Slide 17
03 · ML + FEATURES
14 / 32
Upper-confidence-bound acquisition for active learning
Sequential selection of the next DFT batch [Snoek et al. 2012]
• αUCB(x) = μ(x) + κ · σ(x), with κ = 2
• Posterior mean μ(x) is taken from HistGBR, the more accurate mean predictor on labelled data
• Posterior standard deviation σ(x) is taken from the GPR + RF stack as a calibrated uncertainty source
• κ = 2 balances exploitation (high μ) and exploration (high σ) and is standard in Bayesian optimisation
• Decoupling μ and σ between two models prevents GP underconfidence from suppressing the high-score tail
• Top-N entries by α become the next active-learning DFT batch; returned labels are fed back into both models
SOLARLAB

## Slide 18
03 · ML + FEATURES
15 / 32
Validation under random and grouped cross-validation
5-fold × 5-seed random CV on n = 473 labelled materials
• HistGBR achieves R2 = 0.466 ± 0.035 · MAE = 0.012 · top-20 recall 0.50
• Improves over the prior GPR / GB / ExtraTrees baseline by +50 % in R2 (0.31 → 0.466)
• Ablation: GBR 0.399 · ExtraTrees 0.234 · MEGNet fine-tuned 0.307 · MEGNet frozen 0.366
• Repeated out-of-fold averaging across seeds yields global R2 = 0.492 and top-20 recall 0.50
• Prototype-grouped CV gives R2 ≈ 0, indicating poor extrapolation to unseen structural prototypes
• Chalcogen-family-grouped CV gives R2 ≈ 0.15, with Se the most challenging hold-out
SOLARLAB

## Slide 19
03 · ML + FEATURES
16 / 32
Per-group residual audit
Diagnostic informing the next active-learning batch
• Score = RMSE · √n + 0.02 · (missed top-20), penalising ranking errors at the high-score tail
• Se (n = 182): RMSE 0.042, 17 true top-20 candidates, 9 missed by HistGBR — highest priority
• High-score bin (y > 0.1, n = 14): RMSE 0.145, identifying the under-modelled tail
• Pnma (SG 62, n = 182): RMSE 0.034, 4 of 10 true top-20 missed
• AB2C4 (n = 91): RMSE 0.045, 1 of 7 true top-20 missed
• ABC3 (n = 56): RMSE 0.045, 50 % top-20 miss rate — the most pronounced data-coverage gap
SOLARLAB

## Slide 20
04
CANDIDATES

## Slide 21
04 · CANDIDATES
17 / 32
Top-fourteen candidates (PV score y > 0.10)
All entries are chalcogenides; eleven of fourteen are selenides; AB2C4 is the dominant prototype
• Selenides preferred: 11 of 14 are Se-based and the top six are all Se
• AB2C4 supplies 7 of 14 entries; the remainder is split between ABC3 and ABC2
• Pnma (SG 62) accounts for 7 of 14; remaining entries fall in SG 12, 14, 72 and 15
• PV-score distribution spans 0.10 to 0.49 across the shortlist
• Aggregate descriptors: ⟨Eg⟩ = 1.32 eV · ⟨ε⟩ = 12.5 · ⟨mavg⟩ = 0.58 m0
• 24 % are direct-gap; the remaining 76 % are retained for combined low m*, high ε and low Eb
SOLARLAB

## Slide 22
04 · CANDIDATES
18 / 32
Screening funnel
>105 MP / OQMD → 647 DFT-screened → 473 ML-ready → 41 PV-promising → 14 shortlist
• Stage 1: > 105 structures sourced from Materials Project and OQMD
• Stage 2: 647 candidates with HSE band structure and DFPT dielectric tensor completed
• Stage 3: 473 ML-ready candidates after removing metallic-band and missing-CONTCAR entries (174 excluded)
• Stage 4: 41 PV-promising candidates with composite score y > 0.05
• Stage 5: 14-candidate shortlist with y > 0.10 feeding the next active-learning DFT round
• Funnel narrows by approximately four orders of magnitude into a tractable shortlist for experimental verification
SOLARLAB

## Slide 23
04 · CANDIDATES
19 / 32
Lead candidate — Se16Sn8Zr4
AB2C4 prototype · Pnma (SG 62) · near-optimal Shockley–Queisser gap
• Eg = 1.12 eV, within 0.22 eV of the Shockley–Queisser optimum at 1.34 eV
• mavg = 0.43 m0, indicating low effective mass and high carrier mobility
• εavg = 19.5, providing strong dielectric screening and suppressing Frenkel-exciton formation
• Eb = 7 meV, well below kBT at 300 K, placing the absorber in the Wannier–Mott regime
• Composite PV score y = 0.487, the highest in the screened set
• Sn–Zr–Se ternary phases have reported synthesis routes; no photovoltaic-device demonstration to date
SOLARLAB

## Slide 24
04 · CANDIDATES
20 / 32
Secondary candidate — Cs2Sb6Se2
ABC3 prototype · C2/m (SG 12) · Sb 5s2 lone-pair active cation
• Eg = 1.28 eV, near the Shockley–Queisser optimum
• mavg = 0.81 m0, heavier than the lead candidate but within the device-relevant range
• εavg = 12.6, indicating moderate dielectric screening; Eb = 56 meV
• Composite PV score y = 0.298, complementing the lead candidate from a distinct structural prototype
• Sb 5s2 lone-pair character produces a deep, dispersive valence-band maximum
• Cs–Sb–Se ternary phases have established solution-processing synthesis routes
SOLARLAB

## Slide 25
05
BRIDGE — DEVICE SIM

## Slide 26
05 · BRIDGE
21 / 32
Motivation for device-scale simulation
Bulk material descriptors alone do not determine device-level performance
• DFT delivers Eg, m*, ε and Eb as bulk material-level descriptors
• Device performance additionally depends on stack geometry, contact selectivity, optical absorption and recombination kinetics
• Drift-diffusion coupled to the Poisson equation is required across the full HTL / absorber / ETL stack
• Coherent transfer-matrix-method (TMM) optics are required for thin-film interference [Pettersson et al. 1999]
• Two-dimensional effects (grain boundaries, lateral non-uniformity) cannot be captured in 1D
• Mobile-ion transport must be included to reproduce hysteresis in perovskite-class absorbers
SOLARLAB

## Slide 27
05 · BRIDGE
22 / 32
SolarLab device-simulation framework
1D + 2D drift-diffusion · TMM optics · mobile ions · selective Robin contacts
• Backend: Python solver with FastAPI server-sent events streaming intermediate results
• Frontend: TypeScript / Vite workstation with publication-quality figure rendering
• Numerical scheme: Radau implicit Runge–Kutta with BDF fallback and bisection-in-time on stiff steps
• Optics: coherent transfer-matrix-method using the ASTM G-173 AM1.5G reference spectrum
• Selective contacts: Robin formulation in Sn and Sp, validated against the 1D solver to 6 µV
• Open-source, scriptable and REST-driven; designed for integration into high-throughput screening pipelines
SOLARLAB

## Slide 28
05 · BRIDGE
23 / 32
Drift-diffusion governing equations
Three coupled partial differential equations per absorber layer [Selberherr 1984]
• Electron continuity: ∂n/∂t = (1/q) ∇·Jn + G − R
• Hole continuity: ∂p/∂t = −(1/q) ∇·Jp + G − R
• Poisson equation: ∇·(εr ε0 ∇φ) = −q (p − n + ND − NA + ρion)
• Current densities: Jn = q μn n E + q Dn ∇n · Jp = q μp p E − q Dp ∇p
• Recombination R: Shockley–Read–Hall, Auger and radiative channels; Einstein relation D = (kBT/q) μ
• Generation G: optical generation profile from the TMM model integrated over the AM1.5G spectrum
SOLARLAB

## Slide 29
05 · BRIDGE
24 / 32
Transfer-matrix-method optics
Coherent multi-layer thin-film interference [Pettersson et al. 1999 · Born & Wolf]
• Each layer j is represented by a 2×2 characteristic matrix Lj acting on the tangential (E, H) field components
• Lj = [[cos δj, i sin δj / ηj], [i ηj sin δj, cos δj]]
• Phase thickness δj = (2π / λ) ñj dj cos θj with complex refractive index ñj = n + i k
• System matrix M = L1 L2 … LN yields wavelength-resolved R, T and A
• Generation profile G(x, λ) ∝ |E(x, λ)|2 α(λ), integrated over the AM1.5G spectrum
• Supersedes the Beer–Lambert approximation by capturing interference, back-reflector and interface effects
SOLARLAB

## Slide 30
05 · BRIDGE
25 / 32
Mobile-ion transport
Origin of J–V hysteresis in perovskite solar cells [Calado et al. 2016 · van Reenen et al. 2015]
• Continuity for ion-vacancy density P: ∂P/∂t = ∇·(Dion ∇P + μion P (1 − P / Plim) ∇φ)
• The steric factor (1 − P / Plim) caps ion density at the available lattice-site limit
• Estimated Plim is approximately 1 – 5 % of the cation-site density in MAPbI3
• Ion drift under bias redistributes mobile charge, screens the electric field and modulates the recombination rate
• Couples into the Poisson equation via the source term ρion = q (P − Peq)
• Characteristic time scale of 0.01 – 100 s reproduces the observed scan-rate dependence of perovskite J–V curves
SOLARLAB

## Slide 31
05 · BRIDGE
26 / 32
Selective Robin contact boundary conditions
Surface-recombination boundary conditions in place of Dirichlet pinning
• Left contact: Jn = −q Sn,L (n − neq) · Jp = +q Sp,L (p − peq)
• Right contact: Jn = +q Sn,R (n − neq) · Jp = −q Sp,R (p − peq)
• Contact selectivity: Sn,L ≪ Sp,L yields a hole-extracting (HTL-type) left contact
• Limit S → ∞ recovers the Dirichlet condition (carrier density pinned to equilibrium)
• Limit S → 0 yields a perfectly blocking (zero-flux Neumann) contact
• Captures the surface-recombination physics that SCAPS-1D approximates via Dirichlet pinning
SOLARLAB

## Slide 32
05 · BRIDGE
27 / 32
Capability comparison with SCAPS-1D
Capabilities absent from the SCAPS-1D reference solver [Burgelman et al. 2000]
SOLARLAB

## Slide 33
05 · BRIDGE
28 / 32
1D and 2D solver fidelity comparison
Reference MAPbI3 stack — 50 mV Voc reduction in 2D from grain-boundary recombination
• Stack: spiro HTL 200 nm / MAPbI3 400 nm / TiO2 ETL 100 nm with selective Robin contacts
• 2D variant: a single vertical grain boundary at the lateral midplane of the absorber
• 1D Voc = 0.910 V is reduced to 2D Voc = 0.860 V (ΔVoc = −50 mV)
• The reduction is the grain-boundary recombination channel resolved only by the 2D solver
• 1D models would misestimate device performance by omitting this loss channel
• Solver throughput: a 28-voltage 2D sweep completes in approximately 22 minutes on 4 CPU cores
SOLARLAB

## Slide 34
06
PAYOFF

## Slide 35
06 · PAYOFF
29 / 32
Predicted device J–V for a leading candidate
DFT parameters → device simulation → predicted PCE
• Closes the workflow from > 105 database scan to predicted device-level J–V
• Stack: same spiro HTL / MAPbI3 / TiO2 ETL reference as the 1D-vs-2D run
• Placeholder candidate: MAPbI3 baseline with Voc shifted by +30 mV (~candidate-gap surrogate)
• Real Se16Sn8Zr4 J–V replaces the placeholder once n, k data and DFT parameters are wired into the 2D solver
• Predicted device PCE is the figure of merit relevant for synthesis decisions
• Establishes explicit, falsifiable performance targets for the experimental collaboration
SOLARLAB

## Slide 36
06 · PAYOFF
30 / 32
Outlook
Planned extensions
• Multi-task learning on the ~36 000 PBE gaps in Materials Project to close the prototype-grouped CV gap
• Spectroscopic Limited Maximum Efficiency (SLME) replacing the SQ upper bound, requiring the absorption coefficient α(E) [Yu & Zunger 2012]
• Targeted DFT batch on Se-rich AB2C4 and ABC3 candidates in SG 62, 12, 72 and 15
• Closed-loop automation of DFT batch submission and surrogate re-fitting on label return
• Experimental collaboration to synthesise the top three candidates and feed measured J–V data back into the ML pipeline
SOLARLAB

## Slide 37
06 · PAYOFF
31 / 32
Summary
Principal findings
• Small-sample ML on 473 DFT-labelled materials improves the GPR / GB / ExtraTrees baseline by +50 % in R2
• Fourteen-candidate chalcogenide shortlist; Se16Sn8Zr4 sits near the Shockley–Queisser optimum
• SolarLab 2D drift-diffusion provides the bridge from DFT-derived parameters to predicted device-level J–V
• Compact, physically motivated descriptor and small-sample model identify a tractable subspace under stringent grouped-CV diagnostics
• Experimental collaboration completes the discovery → simulation → experiment loop
SOLARLAB

## Slide 38
06 · PAYOFF
32 / 32
References
ML, device-sim and absorber-chemistry foundations
• Yan C. et al., Nat. Energy 3, 764 (2018) · ACS Energy Lett. 2, 930 (2017) — kesterite Cu2ZnSnS4
• Hou Y. et al., Nat. Energy 5, 131 (2020) · Science 367, 1135 (2020) · Nat. Energy 7, 229 (2022) — perovskite + tandem
• Friedman J.H., Ann. Stat. 29, 1189 (2001) — gradient boosting
• Ke G. et al., NeurIPS (2017) — LightGBM histogram binning
• Rasmussen C.E. & Williams C.K.I., MIT Press (2006) — GP for ML
• Snoek J. et al., NeurIPS (2012) — UCB acquisition
• Ward L. et al., npj Comput. Mater. 2, 16028 (2016) · CMS 152, 60 (2018) — Magpie · matminer
• Heyd J. et al., J. Chem. Phys. 118, 8207 (2003) — HSE06
• Yu L. & Zunger A., PRL 108, 068701 (2012) — SLME
• Selberherr S., Springer (1984) — semiconductor device simulation
• Pettersson L.A.A. et al., J. Appl. Phys. 86, 487 (1999) — TMM
• Burgelman M. et al., Thin Solid Films 361-362, 527 (2000) — SCAPS
• Calado P. et al., Nat. Commun. 7, 13831 (2016) · van Reenen S. et al., JPCL 6, 3808 (2015) — perovskite ion migration
• Chen C. et al., Chem. Mater. 31, 3564 (2019) — MEGNet
SOLARLAB