## Slide 1
SCAPS-1D Main Output Modules
Four primary characterization outputs used to evaluate solar-cell performance, junction electrostatics, defect response, and spectral collection.
editable
SCAPS-1D
A
I-V / J-V characteristics
Chart: 
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1.0 | 1.15 | 1.3
light | 23.8 | 23.7 | 23.2 | 21.7 | 17.2 | 8.4 | 0 | -6.8
dark | 0 | 0 | 0.1 | 0.4 | 1.5 | 5.4 | 15 | 26
Voltage V (V)
Current density J (mA cm−2)
Voc
1.15 V
Jsc
23.8
FF
78%
η
21.3%
light J-V
dark J-V
SCAPS core terminal output: light/dark curves and photovoltaic metrics.
I = J × area; sign convention controls whether the curve appears upward or downward.
B
C-V and Mott-Schottky analysis
Chart: 
| −0.4 | −0.2 | 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1.0
C | 0.92 | 0.82 | 0.7 | 0.59 | 0.49 | 0.42 | 0.38 | 0.37
1/C2 | 0.12 | 0.2 | 0.31 | 0.43 | 0.57 | 0.7 | 0.82 | 0.88
Bias V (V)
Normalized C, 1/C2
Vbi
0.96 V
Neff
2×10¹⁶
C(V)
1/C2
Extract depletion capacitance, built-in voltage, and apparent doping.
Linear 1/C2 versus V is used only in the depletion regime.
Fully depleted thin absorbers need careful interpretation.
C
C-f / admittance spectroscopy
Chart: 
| 10 | 10² | 10³ | 10⁴ | 10⁵ | 10⁶ | 10⁷ | 10⁸
C | 0.95 | 0.94 | 0.91 | 0.83 | 0.63 | 0.42 | 0.31 | 0.28
G | 0.12 | 0.17 | 0.29 | 0.56 | 0.82 | 0.63 | 0.34 | 0.16
Frequency f (Hz)
Normalized C / G
From admittance: Y = 1/Z = G + jωC
C(f)
G(f)
Frequency dispersion indicates slow traps, ions, or interfacial charging.
Temperature-dependent C-f / G-f supports activation-energy analysis.
Here, C-f is derived from impedance/admittance.
D
QE / spectral response
Chart: 
| 300 | 400 | 500 | 600 | 700 | 800 | 850 | 900 | 950
QE | 4 | 35 | 70 | 86 | 88 | 82 | 62 | 20 | 2
Wavelength λ (nm)
QE (%)
QE(λ)
Jsc,QE
23.5
Eg
edge
QE is plotted versus wavelength λ or photon energy hν, not electrical frequency.
Integrated QE gives a consistency check on Jsc under AM1.5G illumination.
Short- and long-wavelength roll-off locate optical and collection losses.
Note: band diagrams, carrier densities, electric field, current components, generation and recombination are diagnostic working-point profiles, not the four primary SCAPS-1D output modules.
Notes: Suggested narration: This slide summarizes the four main SCAPS-1D output modules. I-V/J-V gives terminal photovoltaic performance and dark diode behavior. C-V, usually shown with the Mott-Schottky 1/C^2 plot, extracts built-in voltage and apparent doping under depletion assumptions. C-f/admittance spectroscopy probes frequency-dependent capacitance and conductance, which are often linked to traps, ionic motion, and interfacial charging. QE is the spectral collection response versus wavelength or photon energy and can be integrated to cross-check Jsc. Internal profiles such as band diagrams and recombination profiles are still important diagnostic outputs, but they should be presented separately from these four main modules.