## Slide 1
Representative SCAPS-1D Result Figures
A professional report should connect terminal metrics to spectral collection, band alignment, and spatial loss mechanisms.
editable
SCAPS-1D
A
Terminal J-V and device metrics
Chart: 
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1.0 | 1.1 | 1.2 | 1.3
Light | 24.1 | 24 | 23.8 | 23.3 | 22.2 | 18.4 | 9.2 | 0 | -4.4
Dark × 10 | 0 | 0 | 0.1 | 0.3 | 0.9 | 2.2 | 5.8 | 13 | 24
Voltage V (V)
J (mA cm−2)
light
dark × 10
Voc
1.18 V
Jsc
24.1
FF
78.6%
η
22.3%
Primary performance figure; report scan direction and illumination.
Dark curve diagnoses diode quality, shunt leakage, and series resistance.
B
Spectral response: EQE / QE
Chart: 
| 300 | 400 | 500 | 600 | 700 | 800 | 850 | 900 | 950
EQE | 3 | 34 | 72 | 86 | 88 | 83 | 70 | 24 | 1
Wavelength λ (nm)
EQE (%)
external quantum efficiency
Integrated Jsc,EQE ≈ 23.8 mA cm−2
Short-wavelength drop: front-layer absorption or surface recombination.
Long-wavelength roll-off: absorber band gap and optical thickness.
Use with optical constants to separate reflection and collection losses.
C
Band diagram and quasi-Fermi levels
Chart: 
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700
EC | -3.78 | -3.82 | -3.92 | -3.98 | -4.03 | -4.12 | -4.18 | -4.22
EV | -5.42 | -5.46 | -5.54 | -5.6 | -5.65 | -5.7 | -5.76 | -5.82
EFn | -4.05 | -4.04 | -4.03 | -4.02 | -4 | -3.98 | -3.96 | -3.95
EFp | -5.2 | -5.18 | -5.14 | -5.1 | -5.05 | -5 | -4.96 | -4.92
Position x (nm)
Energy relative to Evac (eV)
EC
EV
EFn
EFp
Band offsets identify transport barriers at ETL/absorber/HTL interfaces.
Quasi-Fermi-level splitting under illumination relates directly to voltage.
A flat or kinked quasi-Fermi level can reveal extraction bottlenecks.
Report at a fixed bias, e.g. V = 0.9 V
D
Loss localization: generation and recombination
Chart: 
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700
G | 1 | 0.78 | 0.61 | 0.48 | 0.38 | 0.3 | 0.24 | 0.19
RSRH | 0.05 | 0.1 | 0.18 | 0.22 | 0.2 | 0.17 | 0.14 | 0.1
Rinterface | 0.04 | 0.08 | 0.18 | 0.75 | 0.26 | 0.12 | 0.08 | 0.05
Position x (nm)
Normalized rate
G
RSRH
Rinterface
Compare where photons create carriers with where carriers are lost.
Sharp interface peak suggests defect-rich or misaligned junction loss.
Pair with current profiles to check whether loss is transport- or recombination-limited.
Use for: loss diagnosis and stack optimization
Takeaway: SCAPS-1D figures should link terminal metrics to optical collection, band alignment, and recombination-loss localization.
Notes: Suggested narration: This slide shows professional SCAPS-1D result figures rather than generic curve sketches. The J-V panel reports terminal performance and diagnostic dark behavior. The EQE panel shows spectral collection and integrated current. The band diagram connects material parameters and interface band offsets to extraction barriers and quasi-Fermi-level splitting. The generation/recombination panel localizes where carriers are created and where they are lost, which is essential for identifying whether the device is limited by optics, transport, bulk recombination, or interface recombination.