## Slide 1
Perovskite Solar Cell Simulator
Technical Deep Dive: Implementation & Architecture
perovskite-sim
March 2026

## Slide 2
Agenda
System Architecture & Module Overview
Spatial Discretization: Tanh-Clustered Grids & Scharfetter-Gummel Scheme
Physics Modules: Poisson, Continuity, Recombination, Ion Migration
Solver Architecture: Method of Lines & Initialization Strategy
Operator Splitting Fallback for Stiff Dynamics
Simulation Experiments: J-V, Impedance, Degradation
Correctness Issues & Future Improvements
Summary & Key Takeaways

## Slide 3
System Architecture
discretization/
• grid.py
• fe_operators.py
physics/
• poisson.py
• continuity.py
• recombination.py
• generation.py
• ion_migration.py
solver/
• mol.py
• newton.py
• illuminated_ss.py
experiments/
• jv_sweep.py
• impedance.py
• degradation.py
models/
• parameters.py
• device.py
• config_loader.py

## Slide 4
Spatial Discretization

## Slide 5
Tanh-Clustered Grid
Formula: ξᵢ = tanh(α·ξ̃ᵢ) / tanh(α)
Parameter: α = 3.0
Purpose: Concentrate grid points near device boundaries (junctions)
Key Feature: Points cluster at interfaces where physics is stiff
Implementation: multilayer_grid concatenates per-layer grids, dropping duplicate interface nodes
Grid Clustering Pattern:
Coarse spacing in bulk
↓ ↓ Dense clustering ↓ ↓
Left junction
↓ ↓ Dense clustering ↓ ↓
Coarse spacing in middle
↓ ↓ Dense clustering ↓ ↓
Right junction

## Slide 6
Scharfetter-Gummel (SG) Scheme
Bernoulli Function
B(x) = x / (eˣ - 1)
Electron Flux
Jₙ = qDₙ/h [B(ξ)·nᵢ₊₁ - B(-ξ)·nᵢ]
Key Properties & Implementation
✓ Exact solution for linear potential within each element — no artificial diffusion
✓ Numerically stable: uses Taylor series for |ξ| < 1e-8 to avoid overflow
✓ Vectorized over all N-1 cell faces for efficiency
✓ Maintains charge conservation naturally through continuity equations

## Slide 7
Physics Modules

## Slide 8
Poisson Equation Solver
Method: Finite-volume discretization on dual grid
Solver: Sparse tridiagonal system in scipy CSR format
Boundary Conditions: φ(0) = 0 and φ(L) = V_bi - V_app
Performance: Tridiagonal structure → O(N) solve time

## Slide 9
Carrier Continuity Equations
Continuity Equation: ∂n/∂t = -(∂Jₙ/∂x) + G - R
Electron Flux: Vectorized Scharfetter-Gummel at all N-1 cell faces
Generation: Optical generation from Beer-Lambert law
Recombination: SRH + radiative, computed per cell
Interface Handling
Boundary nodes (contacts) held fixed at equilibrium values
Harmonic-mean diffusivity at inter-layer interfaces
Dual-grid finite-volume conserves charge across layers
Automatic handling of heterojunction discontinuities

## Slide 10
Recombination Mechanisms
SRH (Shockley-Read-Hall)
R_SRH = (np - ni²) / [τp(n+n₁) + τn(p+p₁)]
Trap-assisted recombination via mid-gap states. Dominant loss mechanism in perovskite bulk. τn = τp = 1 μs for MAPbI₃.
Radiative
R_rad = B_rad · (np - ni²)
Bimolecular band-to-band recombination. B_rad ≈ 5×10⁻²² m³/s for MAPbI₃. Important near open-circuit conditions.
Auger
R_Auger = (Cn·n + Cp·p)·(np - ni²)
Three-particle high-injection process. For perovskites: C ~ 10⁻⁴² m⁶/s — negligible under normal operation.

## Slide 11
Ion Migration (Steric Blakemore Model)
Steric-Corrected Flux
F_P = -D_I · (∂P/∂x) / (1 - P/P_lim) + (D_I/V_T) · P · (∂φ/∂x)
Key Parameters:
P_lim: 1.6 × 10²⁷ m⁻³
D_ion: 1 × 10⁻¹⁶ m²/s
V_T: kT/q ≈ 26 mV @ 300 K
Steric Factor:: (1 - P/P_lim)⁻¹
Boundary Conditions
Zero-flux at bulk boundaries
Confines ions to device interior
No injection or extraction at contacts
Prevents spurious ion accumulation
Maintains charge neutrality in bulk

## Slide 12
Solver Architecture

## Slide 13
Method of Lines (MOL)
State Vector: y = [n, p, P] (3N components, where N = number of grid points)
assemble_rhs(t, y):
1. Unpack y → n(x,t), p(x,t), P(x,t)
2. Apply BCs Set boundary values (equilibrium at contacts)
3. Poisson Solve φ(x,t) from ∇·(ε∇φ) = q(p - n + P + N_D - N_A)
4. Generation G = α(λ) · e^(-αx) · Φ_incident
5. Continuity ∂n/∂t = -(∂Jₙ/∂x) + G - R, ∂p/∂t = +(∂Jₚ/∂x) + G - R
6. Ion Migration ∂P/∂t = -(∂F_P/∂x)
7. Pack dy/dt = f(t, y)
Integrator: Radau IIA 5th order (implicit) | rtol=1e-4, atol=1e-6 | Handles stiffness from ion dynamics

## Slide 14
Two-Step Initialization Strategy
Step 1: Quasi-Neutral Equilibrium
Module: newton.py
Equations:
• n·p = nᵢ²
• n - p = N_D - N_A + P
Closed-form solution (no iteration)
Overflow-free across multiple layers
(nᵢ spans 10 orders of magnitude)
Sets n, p, P at t=0
Step 2: Illuminated Settling
Module: illuminated_ss.py
Duration: 1 ms transient
Under light illumination
(generation turned on)
Ions frozen (P held constant)
Eliminates dark→light artifact
Carriers settle to quasi-equilibrium
with optical generation

## Slide 15
Operator Splitting Fallback
When: Radau fails (ion pile-up at interfaces, stiffness ratio > 10⁸)
Phase 1: Ion Advance
Freeze n, p
(carrier distribution held)
Advance P only (ions)
via Radau
Less stiff ODE system
(simpler eigenvalues)
Module: mol.py
Phase 2: Carrier Re-equil.
Freeze P (ions now fixed)
Quick transient: 1 µs
Carriers relax to new
quasi-Fermi levels
With updated ion field
Repeat until convergence
Diagnostic: Clipping counter warns on numerical instability (unphysical ion densities or negative carriers)

## Slide 16
Simulation Experiments

## Slide 17
J-V Sweep with Hysteresis
Module: jv_sweep.py
Voltage Protocol:
Forward: V = 0 → V_bi (open circuit)
Reverse: V = V_bi → 0
Time per Voltage Step: One carrier lifetime (τ ~ 1 µs)
Illumination: AM1.5G spectrum, constant
Output Metrics:
• V_oc: Open-circuit voltage
• J_sc: Short-circuit current
• FF: Fill factor
• PCE: Power conversion efficiency
Hysteresis Index
Definition:
HI = (PCE_reverse - PCE_forward) / PCE_reverse
Quantifies difference between forward and reverse scans
In perovskites, caused by ion migration and charge redistribution
Positive HI indicates forward scan yields lower PCE
Diagnostic tool for ion dynamics validation

## Slide 18
Impedance Spectroscopy (EIS)
Measurement: Small-Signal AC Perturbation Around DC Bias
AC voltage: V(t) = V_DC + ΔV·sin(ωt) where ΔV = 0.01 V, f = 10⁻³ to 10⁶ Hz
DC Bias Step
Establish initial conditions
1 ms transient settling
Ions and carriers reach quasi-equilibrium
Lock-in detection baseline
AC Perturbation
Frequency sweep: 10 Hz → 1 MHz
Phase-sensitive detection
Extract real & imaginary impedance
Lock-in reference from midpoint time
Output: Nyquist Plot
Z(f) = Z_real - i·Z_imag
Semicircles reflect R-C layers
Arc radius → interface resistance
Eliminates phase bias artifacts

## Slide 19
Long-Term Degradation Simulation
Module: degradation.py
Conditions:
• Voltage: Constant bias (e.g., V_app = 0.8 V)
• Illumination: AM1.5G spectrum (constant)
• Duration: Long-term integration (hours to days simulated)
Sampling:
• Snapshots: Log-spaced time points for efficiency
• Metrics per snapshot: V_oc, J_sc, FF, PCE, ion distribution
V_oc Calculation: Geometric-mean quasi-Fermi separation: V_oc = (E_F^n - E_F^p) / q
Fallback: Operator splitting activated if Radau fails (ion pile-up)
Output: Degradation curves: PCE vs. time, V_oc vs. time, etc.

## Slide 20
Correctness Issues Found
⚠ AMBER: Duplicate Q (elementary charge) constant definitions in multiple modules — maintenance risk
🔴 CRITICAL: Beer-Lambert illumination direction wrong for n-i-p devices — light enters from left but n-i-p absorbs from ETL (right); 1/e depth ~77 nm makes spatial profile impact significant
⚠ AMBER: Ion D_ion applied uniformly across entire device — should vary per-node; may allow spurious ion diffusion into transport layers
ℹ INFO: Degradation PCE is proxy (V_oc only) — overestimates by ~100–150 mV, lacks FF effects; full J-V curves needed for accuracy

## Slide 21
Summary & Key Takeaways
Robust Numerics:
✓ Scharfetter-Gummel fluxes (exact for linear potential)
✓ Radau IIA implicit time integration (handles 10+ orders of stiffness)
✓ Sparse tridiagonal Poisson solver
Multi-Layer Architecture:
✓ Per-layer material parameters
✓ Harmonic-mean interface treatment for permittivity and diffusion coefficients
Ion Physics:
✓ Steric Blakemore model with excluded-volume correction
✓ Operator splitting fallback for stiff ion dynamics
✓ Zero-flux confinement boundary conditions
Validation:
✓ ~50 unit tests, integration tests (np = ni² at equilibrium)
✓ Regression tests for physical plausibility (J_sc, V_oc, FF ranges)